## Slide 1: USING GAMMA-RAY AND X-RAY COMPUTED TOMOGRAPHY FOR POROSITY QUANTIFICATION OF RESERVOIR ANALOGUE ROCKS
ABRAÃO NOVA, FREDERICO RIBEIRO, PAMALLA OLIVEIRA, DANIEL AMANCIO, CÁSSIA MACHADO, ALEXANDRA CAROLINA, MARCIO PAIXÃO, ANTONIO ANTONINO, ENIVALDO BARBOSA, ANTONIO BARBOSA, MARIA LOURENÇO, MARCOS RODRIGUES, AND RICHARD HECK
#shareEGU20

## Slide 2
X-ray micro-computed tomography (µCT)
Characterization of rock properties
High-resolution 3D digital images.
Porous systems in reservoir rocks.
1
Introduction
#shareEGU20

## Slide 3
#shareEGU20
#shareEGU20
a) Imagem em HU
b) Huang
c) IsoData
d) Li
e) Moments
e) Otsu
e) PVE
The challenge:
Reliable quantification of porosity in rocks which present pore sizes ranging from centimeter to nanometer scale;
Intrinsic limits of the x-ray imaging method.
1
Introduction

## Slide 4
Problems that are related to the physical aspects of the µCT imagem Method:
Image artifacts;
Bam hardening effect.
#shareEGU20
#shareEGU20
Ring Artifact
Beam hardening effect
1
Introduction

## Slide 5
The computational costs of processing for large image volumes, necessary for the reliable definition of some petrophysical characteristics of rock samples, like porosity and permeability.
#shareEGU20
1
Introduction

## Slide 6
A method is presented for quantification of porosity, based in data from gamma ray tomography. The objective was to create a protocol for core samples scanning in a gamma tomograph, in order to perform porosity calculation with reliable results within the minimum operational time.
The study was carried out in in sandstones and limestones samples (bioclastic mudstones and wackstones)
The results obtained was compared with the porosity quantification results produced with the application of traditional segmentation methods in µCT images of the same samples. Also, the results of gamma tomography and µCT images analyses were compared with porosity data obtained with a porosimeter for the same samples.
The traditional hard-data obtained with the porosimeter was used as a reference to compare with the other two sets of results.
2
Objective
#shareEGU20

## Slide 7
These analyses were performed in core samples of limestones and sandstones analogous of Brazilian oil reservoirs.
#shareEGU20
Sandstone cores from Botucatu Fm
Bioclastic limestones
(wacstones and packstones)
from Jandaira Fm
Sample | Diametre (cm) | Length (cm)
B1 | 2.54 | 4.44
B2 | 2.54 | 4.19
C1 | 2.54 | 3.68
C2 | 2.54 | 4.04
Materials and Methods
3
Samples dimension

## Slide 8
#shareEGU20
Core
XR-µCT
Imaging
Rγ-CT
scaning
Radiodensity/Histogram evaluation
Attenuation Coefficient
Porosity
Basic Workflow for Evaluation of Samples
Image Segmentation
Materials and Methods
3

## Slide 9
Gamma Ray attenuation method
#shareEGU20
(a) Radioactive source;
(b) Reference sample without pores;
(c) Detector;
(d) Porous rock sample.
Experimental procedure for determining porosity with the Gamma Ray attenuation method
Materials and Methods
3

## Slide 10
#shareEGU20
Porosity
NIST XCOM
Data
Mineral
Density
Data
Linear
Attenuation
Coefficient
of Minerals
γ-Ray CT
Linear
Attenuation coefficient of the Samples
Sample
Thickness
2
Materials and Methods

## Slide 11
#shareEGU20
Rock
Sample
Detector
Gamma radiation beam
Radiation Source
Scan direction
Shielding and
collimator
Shielding and
collimator
Radiation Source: 137Cs (662 keV);
Half-life: 30,1 years;
Radioactive activity: 3.70x109 Bq;
NaI(Tl) Scintillation Crystal Detector
Lead collimator with circular hole 5.5 mm in diameter and length 73 mm.
2
Materials and Methods
Gamma-Ray CT

## Slide 12
135º
0º
45º
90º
16 points in each plane
Axial view
#shareEGU20
Distant by 1 mm
Axial view
Materials and Methods
3

## Slide 13
#shareEGU20
Scan Parameter | Value
Electric current (µA) | 70 µA
Maximal tension (kV) | 150 kV
Aluminum Filter | 0.25 mm
Voxel Resolution | 30 µm
Integration time | 500 ms
X-RAY µCT Scan Parameter
Materials and Methods
3
X-Ray CT
Grayscale image

## Slide 14
#shareEGU20
X-RAY µCT image
Croped ROI
Binary image
Sample | Threshold
B1 | 1325
B2 | 1325
C1 | 2630
C2 | 2630
PVE segmentation
Materials and Methods
3

## Slide 15
4
Results and Discussion
#shareEGU20
C
B
Chart: Porosity, He (%)
| 26.518139999999999 | 24.150739999999999 | 33.732689999999998 | 35.802349999999997
γR-CT (%) | 28.5053 | 27.8299 | 40.7937 | 40.7937
µCT-RX (%) | 20.36 | 20.13 | 33.7 | 32.15
Sample | Porosity (%) |  | 
 | γR-CT | XR-µCT | He
B1 | 28.51 | 20.36 | 26.52
B2 | 27.83 | 20.13 | 24.15
C1 | 40.79 | 33.70 | 33.73
C2 | 40.79 | 32.15 | 35.80

## Slide 16
Scan time around 25 min
Volume reconstruction around 15 min
Image segmentation and porosity arond 60-120 min
#shareEGU20
γR-CT | XR-µCT | He
30 min | 2-3 hour | 5 min
It Is an experimental approach
What is important in this new approach is to test the possibility
of obtaining activated pore measurements, in less time and cost,
than in the extreme two methods
Time required in each methodology
4
Results and Discussion

## Slide 17
The results suggest that Industrial application of γ-ray CT for precise evaluation of large number of core samples can be highly effective. The method allows the porosity quantification of a larger number of cores, with less operational and computational costs.
Furthermore, the γ-ray data can be integrated with data provided by conventional X-ray µCT image processing to complement information regarding morphological aspects. This can be done for a fewer number of cores, due the higher complexity of this process and costs in terms of time and computation.
4
Conclusion
#shareEGU20

## Slide 18
6
Acknowledgment
#shareEGU20

## Slide 19: Thank you!
#shareEGU20
abe.alves2@gmail.com
Abraão Alves Vila Nova
Department of Nuclear Energy - Federal University of Pernambuco – Brazil

## Slide 20: Using Gamma-Ray and X-Ray Computed Tomography for Porosity Quantification of Reservoir Analogue Rocks
Abraão Nova, Frederico Ribeiro, Pamalla Oliveira, Daniel Amancio, Cássia Machado, Alexandra Carolina, Marcio Paixão, Antonio Antonino, Enivaldo Barbosa, Antônio Barbosa, Maria Lourenço, Marcos Rodrigues, and Richard Heck
#shareEGU20