## Slide 1
METHODS FOR THE ANALYSIS OF ASBESTOS IN INCOHERENT SOILS
Giovanna Zanetti
Oliviero Baietto
Paola Marini
Politecnico di Torino,
Department of Environment, Land and Infrastructure Engineering (DIATI)

## Slide 2
SOILS CONTAMINATED WITH ASBESTOS
ANTHROPOGENIC
NATURAL

## Slide 3
TECHNOLOGY | USE | LIMITS | RESOLUTION
DRX X-Ray Diffraction | Asbestos weight determination | Concentration >1% | 
IR Infrared Spectroscopy | Asbestos weight determination | Concentration >1% | 
SEM Scanning Electron Microscopy | Asbestos weight determination Determination of airborne fibre number concentration | Concentration >0,1% (Quantitative) 0,01%< Concentration>0,1% (semi-quantitative) | 5 nm
PCOM Phase Contrast Optical Microscopy | Asbestos QUALITATIVE determination Determination of airborne fibre number concentration (not used) | Concentration < 1% Fiber diameter > 0,3 μm | 0,2 μm
ITALIAN LAW IN FORCE FOR ASBESTOS QUANTIFICATION: DM 6/9/94

## Slide 4
PCOM
Macroscopic observation
If it is possible perform a manual sorting. If the concentration of asbestos is greater than 1000mg/Kg the analysis is finished
ANALYSIS METHODOLOGY
1/7
2/7
Quartering and classification of the sample (100/120 gr) into 4 grain size classes. (sieves: 0.6 mm; 0.3 mm; 0.15 mm; 0.075 mm)
3/7
Preparation of weighed slides using oils with note refractive index
4/7

## Slide 5
Recognition of different kind of asbestos thanks to their characteristic optical properties
Observation and measuring (length,diameter) of the asbestos fibers on a fixed number of fields
5/7
6/7
Determination of the asbestos content obtained by the relationship between the weights of the fibrous component compared to the granular ones.
7/7
PCOM
ANALYSIS METHODOLGY

## Slide 6
EXAMPLE OF ASBESTOS VISION
RECOGNITION ON THE MICROSCOPIC SLIDE
n=1.550
0,6-0,3 mm
Mass on the slide = 80 mg

## Slide 7
SEM
Comminution of the sample until the granulometric spectrum
is in the range between 10 and 100 μm
Dispersion of a known amount of a powder sample (10 mg) in a known volume of a solution (200 ml) (with surfactant) and put it in a ultrasonic bath
ANALYSIS METHODOLGY
1/7
2/7
Filtration of a part of the suspension (7,5 ml/0,375 mg)
on a polycarbonate filter
3/7
Place a portion of the membrane on the stub for SEM analysis and coat it with Au using a Sputter Coater
4/7
SEM analysis is used for grain size classes less than 0.15mm

## Slide 8
Observation, at a proper magnification, of a number of microscopic fields adequate to the limit of detection
Identification of the asbestos fibres by morphology and X-ray dispersion energy spectroscopy (EDS), and measure of their dimensions
5/7
6/7
Determination of the asbestos content obtained by the relationship between the weights of the fibrous component compared to the one granular.
7/7
SEM
ANALYSIS METHODOLGY

## Slide 21: Conclusions
All HSL samples were analyzed with an optical microscope, although the quantities of asbestos contained in the sample were small. This was possible because the fibers were large enough to be observed. Optical microscopy allowed us to observe a more representative sample.
Certainly if we had finished the analysis with the SEM observation of the smaller particle size classes, the results would have been better.
We could also try to read the samples only at SEM, but I fear that, being relatively large fibers, the results may be incorrect without observing a representative sample.