## Slide 1
The Granite of Pena, the Building Stone of the Most Important Buildings of the Twentieth Century in Vila Real (Northern Portugal)
Dr. David Martín Freire-Lista
Dr. Luís Sousa
Dr. Martinho Lourenço
European Geosciences Union
General
Assembly
2020
Heritage Stones: Global relevance vis-à-vis architectonic heritage

## Slide 2
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
Geosciences center
University of Coimbra
University of Tras-os-Montes e Alto Douro
Geology deparment
General
Assembly
2020

## Slide 3
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020
Vila Real

## Slide 4
Diogo Cão House , 15th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 5
Mateus Palace, 18 th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 6
Nossa Senhora da Pena Sanctuary, 18th century
São Paulo Church, 18 th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 7
Justice Court, 20th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 8
Post house, 20th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 9
Seminary, 20th century
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 10
Coat of arms
0
20
cm
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 11
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 12
AIMS
RESULTS
CONCLUSIONS
INTRODUCTION
1 Locate the historical quarries
2 Characterise the extraction area
2.1 Historic quarry modeling
2.2 Cartography of the extraction area
2.3 Volume of extracted granite
3 Characterise the building stones
3.1 Petrographic properties
3.3 Petrophysical properties
3.3.1 Hydric properties
3.3.2 Ultrasound pulse velocity
3.3.3 Colour
3.2 Mineralogical composition (XRD)
DECAY
General
Assembly
2020

## Slide 13
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
The Portuguese Geographic Dictionary of 1747 indicates that in Pena, a village near Vila Real city, there is good “Pedra mármore”
1 Locate the historical quarries
General
Assembly
2020
Notes: Historic building materials were typically near the place where they would be used. The geology of Northern Portugal is broadly composed of metamorphic rocks and granites. Each stone had a use according to its aesthetic and durability characteristics. These materials have created a rich cultural heritage that has been preserved up to this date.
Industrialisation, the development of means of transport and new materials have led to the abandonment of historical quarries, necessary for the conservation of monuments. The location of these quarries allows the creation of open-air museums and walking routes. In addition, the use of their stones for restoration will guarantee the supply for future generations, promoting local employment and the conservation of built heritage, both rural and urban heritage in a specific area.
Documentary search, cartography and petrographic characterisation are necessary to locate the historical quarries of the stones with which monuments have been built. The use of drones together with topographic analyses allows geologists to know the approximate granite volume extracted from the historical quarries, to calculate reserves and to locate granite boulders that can be used in future restorations. The use of analytical techniques, such as petrography, accelerated artificial ageing, ultrasound pulse velocity measurements and spectrophotometry will guarantee the quality, durability and colour of restoration stones. In addition, tourist routes with information panels and QR codes from the historic buildings to the original quarries of their building granites will allow visitors to know about the local heritage, geology and landscape of the area.
The implementation of this project aims at the revitalisation of villages with quarrying tradition and at the sustainable conservation of cultural heritage, inventorying building granites that can be used for restoration and creating a proximity trade. Restoration stones needs will be guaranteed without compromising their supply for future generations.
The period of most intense development of traditional stonework in the Trás-os-Montes area occurred in the 18th century. The Portuguese Geographic Dictionary of 1758 indicates that in Pena, a village near Vila Real city, capital of the homonymous district, there was “pedra mármore”, a leucogranite of fine crystal-size, white colour and with extraordinary petrophysical characteristics. In addition to the discovery of these quarries, an important historical quarry of granite with coarse crystal-size was discovered in the highest mountain of this village, from where an extraordinary panorama of Vila Real city can be admired.
Pena retains numerous vestiges of historical stonework and a profuse use of it. There are numerous door lintels that retain the construction date carved on them, as well as houses with carved ashlars, granite pinnacles, granaries and roadside granite crosses. The lintels and jambs of the doors and windows of its parish church were carved out of “pedra mármore”, while the walls and crosses dating from the 18th century and arranged on its perimeter were built with the coarse crystal-size granite. More recently, the seminary was built with Pena granites. In addition, the court and post office buildings also in Vila Real, were also built with Pena granites.

## Slide 14
Church of Sao Miguel da Pena
Picarreira montain
1 Locate the historical quarries
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 15
1:50.000
0
1
Km
Metasedimentary
rocks
Vila Real granite
Aplites
1 Locate the historical quarries
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020
Notes: Intrusive rocks

## Slide 16
Drone: DJI phantom 4
Flight planning and navigation software: Fix 4D Capture
Coverage: Double mesh
Photo overlay: 80 %
Flight height: 50 meters of the take-off
Model / Photogrammetric Processing: AGISOFT METASHAPE
2 Characterisation of the extraction area
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 17
Hydric properties: UNE-EN 1936: 2007
Natural stone test methods.
3.3.1 Hydric properties
Bulk density and effective porosity
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 18
3.3.2 Ultrasound pulse velocity
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 19
3.3.3 Colour
Dry
Wet
X-Rite colorimeter (model 964).
Illuminant: D65
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020
White
Black
Green
Red
Yellow
Blue
Notes: X-Rite colorimeter (model 964) (Fig. 6a), with a 45°/0° geometry and specular component included, and by using the D65 illuminant. Considering the polyphasic character and textural heterogeneity of the stones, several shots must be done to get a mean value (Prieto et al. 2010, Urosevic et al. 2010, Sousa and Gonçalves 2012). In this study,
The colour parameters were obtained from the mean value of 20 shots made with the 8 mm aperture.
Colour is expressed using CIE-L*a*b* system, the most widely used to classify the colour without misinterpretations. In the CIE-L*a*b* system, the colour is quantified according to three chromatic coordinates.
The L* parameter represents lightness or luminosity (L*=0, black; L*=100, white).
the a* parameter is the red–green axis (a*>0, red; a*<0, green)
the b* parameter is the yellow–blue axis (b*>0, yellow; b*<0, blue).

## Slide 20
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
2 Characterisation of the extraction area
616.2 m
429.2 m
General
Assembly
2020

## Slide 21
2 Characterisation of the extraction area
Old road
Stone dumps
Stone stockpile
Extraction Zone
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 22
0
1
mm
3.1 Petrographic Properties
Granite
Qzt
Qzt
Qzt
Mo
Mo
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 23
3.1 Petrographic Properties
0
1
mm
Aplite
Qzt
Qzt
Qzt
Mo
Mo
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 24
Quartz
Albite
Muscovite
Oligoclase
Microcline
3.2 Mineralogical Composition (XRD)
GRANITE
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 25
Quartz
Albite
Muscovite
Oligoclase
Microcline
×
3.2 Mineralogical Composition (XRD)
APLITE
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 26
3.3.1 Hydric properties
Aplite
Granite
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 27
3.1.2 Ultrasound pulse velocity
 |  | Vp (m/s) |  |  | 
 | Granite | 3978 | ± | 180 | 
 | Aplite | 4567 | ± | 108 | 
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION

## Slide 28
3.1.3 Colour
Aplite
Dry |  |  | Wet (1h) |  | 
L | a* | b* | L | a* | b*
67.66 | 0.61 | 8.05 | 51.24 | 1.03 | 10.95
63.04 | 3.8 | 13.41 | 42.24 | 7.51 | 19.01
b
a
Granite
Granite
Aplite
3.3 Petrophysical properties
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
General
Assembly
2020

## Slide 29
MATERIALS & METHODS
RESULTS
CONCLUSIONS
INTRODUCTION
The quarries of Pena have supplied building stones for Vila Real heritage buildings.
Two types of igneous stones are the most used in the built heritage of Vila Real: granite and aplite.
Both building stones have different petrophysical properties and similar mineralogical composition.
The stone decay will be studied with accelerated artificial aging tests.
General
Assembly
2020

## Slide 30
THANK YOU FOR YOUR ATTENTION
Dr. David Martín Freire-Lista
davidfreire@utad.pt
General
Assembly
2020
Heritage Stones: Global relevance vis-à-vis architectonic heritage