## Slide 1
Examining saturated and unsaturated hydraulic parameter changes as a result of geochemical reactions in tailings
R. Akesseh1, M. Edraki2 and T. Baumgartl3,4
1PhD student, Sustainable Minerals Institute, The University of Queensland, St Lucia QLD 4069, r.akesseh@uq.edu.au
2Principal Research Fellow, Sustainable Minerals Institute, The University of Queensland, St Lucia, QLD 4069. m.edraki@cmlr.uq.edu.au
3Director, Geotechnical and Hydrogeological Engineering Research Group (GHERG), Federation University Australia, Gippsland VIC 3841, t.baumgartl@federation.edu.au
4Honary Professor, Sustainable Minerals Institute, The University of Queensland, St Lucia QLD 4069. t.baumgartl@uq.edu.au
1. INTRODUCTION
Water flow and solute transport in the unsaturated zone is governed by the hydraulic properties and the hydraulic conductivity function. However, geochemical reactions induce changes in the hydraulic properties as oxidation occurs in reactive materials. Transient flow experiment can be designed to indirectly estimates these changes. This is an easy and practical method which relies on easily measureable parameters. Our aim was to test the hypothesis of induced hydraulic properties changes due to geochemical reaction using inverse numerical modelling.
2. HYDRAULIC PROPERTIES ESTIMATION
One dimensional vertical flow in rigid porous media is governed by Richards equation,
Initial and Boundary condition
Van Genucten-Mualem hydraulic function
INVERSE ANALYSIS
Hydraulic parameters α and n determined by minimisation of objective function
Solution by Levenberg-Marquardt algorithm
Solution was implemented in HYDRUS-1D
3. MATERIALS AND METHODS
Material Composition
  Dolomite (25%)
  Pyrite (25%)
  Quartz (35%)
  Chlorite (15%)
Two categories of particle size range
  <75 µm
  75-200 µm
Column: 4 cm, bulk density: 1.4 g/cm3
Nine drying and wetting cycles over nine months
Initial hydraulic parameters determined by desiccation
Curve fitting in RETC
Transient water flow experiment by evaporation
Mass of water loss was measured by a balance
Hydraulic conditions in the tailings measured by tensiometer
4. RESULTS
Fig 2: Cumulative water loss vs time
Fig 6: Comparison of initially measured hydraulic parameters and inversely measured parameters
Fig 5: Plot of inversely modelled hydraulic conditions in the column
Fig 4: Initial water retention curve for different particle sizes
Fig 3: Time series of hydraulic condition in the column
Fig 1: Evaporation Experiment
5. CONCLUSION
The model results show that hydraulic parameters of the studied material changed over time
The inverse model was effective in establishing these changes
On the assumption of the saturated volumetric and saturated conductivity decreased by 1% during this period the alpha and n parameters of the coarse and fine material changed with time
REFERENCES
NAKHAEI, M., ŠIMŮNEK, J. J. J. O. H. & HYDROMECHANICS 2014. Parameter estimation of soil hydraulic and thermal property functions for unsaturated porous media using the HYDRUS-2D code. 62, 7-15.
ROMANO, N. & SANTINI, A. 1999. Determining soil hydraulic functions from evaporation experiments by a parameter estimation approach: Experimental verifications and numerical studies. Water resources research, 35, 3343-3359.
ŠIMŮNEK, J., VAN GENUCHTEN, M. T. & WENDROTH, O. 1998. Parameter estimation analysis of the evaporation method for determining soil hydraulic properties. Soil Science Society of America Journal, 62, 894-905.
TOORMAN, A., WIERENGA, P. & HILLS, R. 1992. Parameter estimation of hydraulic properties from one‐step outflow data. J Water Resources Research, 28, 3021-3028.
Parameter | Initial value |  | Optimised value | 
 | Fine | Coarse | Fine | Coarse
(cm/day | 1.06 | 128.76 | 1.05 | 127.47
) | 0.7 | 0.64 | 0.69 | 0.63
 | 0.19 | 0.07 | 0.19 | 0.07
n | 1.78 | 7.36 | 1.36 | 2.09
 | 0.007 | 0.01 | 0.0013 | 0.026
Parameter | Initial value |  | Optimised value | 
 | Fine | Coarse | Fine | Coarse
 | 1.06 | 128.76 | 1.05 | 127.47
 | 0.7 | 0.64 | 0.69 | 0.63
 | 0.19 | 0.07 | 0.19 | 0.07
n | 1.78 | 7.36 | 1.36 | 2.09
 | 0.007 | 0.01 | 0.0013 | 0.026
Table 1: Initial parameter and optimised values after changes