## Slide 1: The role of calcium diffusion on high temperature SO₂ uptake by volcanic glasses
2
6
7
Ana S. Casas¹, Fabian B. Wadsworth², Paul M. Ayris¹, Pierre Delmelle³, Jeremie Vasseur¹, Corrado Cimarelli¹, and Donald B. Dingwell¹
SEM, BET analysis
Particle size distribution
References
2) Ayris et al., 2015 Bull Volcanol
3) Tuffen and Castro 2009 J Volcanol Geotherm Res
ana.casas@lmu.de
1) Calc alkaline rhyolite³ (natural)
2) HPG8¹ +1-2wt% CaO + 0-2.5wt%FeO
Temperature
Grain size distribution
Exposure time
200, 300, 400, 500, 600, 700 and 800°C
<63, 63-90 and >90 µm
1, 3, 5, 15, 30 and 60 min.
Samples
Variables
IC analysis
Leaching (1:250 ratio)
20
40
50
60
70
0.0
0.2
0.4
0.6
0.8
1.0
R(µm)
90-63
<63
0.0
Normalized concentration, Ca/Cᵢ
D(m² s⁻¹)
>90
.
10
-15
2.66
10
.
.
-15
1.62
10
.
-15
1.52
1) Casas et al., 2019 Geochim. Cosmochim. Acta
Chaitén 2008 dome
Methods: high temperature SO₂-glass interactions
2
Future work
Our final goal is enable the modelling of high temperature SO₂ uptake by a given eruption. By knowing the mechanisms and variables controlling Calcium diffusion, we can modify the model of Suzuki et al. (2005)⁵ and predict the mass of SO₂ within an eruption.
7
5
Discussion
Introduction
Our work has also shed light into the mechanisms and parameters involved in volcanic gas uptake; chemisorption from SO₂, followed by CaSO₄ growth on the glass surfaces prompts the process, this drives a chemical potential induced-diffusion of Ca²⁺ which results in subsequent CaSO₄ growth.
SO₂ high-temperature uptake by glass (from ash) has been studied and recognized to be an effective process to remove SO₂ from the atmosphere during large volcanic eruptions¹.
Another interesting observation, was that the Fe³⁺/ΣFe ratio of the glass increases with increasing temperature and is almost directly proportional to the Ca²⁺ diffusion, leading to the hypothesis that both Ca²⁺ diffusion and Fe²⁺ oxidation are linked in as a cause/effect of SO₂ uptake.
1
T [°C]
Signal (a.u.)
Signal (a.u.)
KeV
KeV
4
Microprobe analysis
Fe3+/Fe2+ ratio
determination
Potentiometric K2Cr2O7 titration
Characterization
Advanced Ash-Gas Reactor²
3
Results: SO₂ turns into CaSO₄ on sample surfaces
IC Analysis
Showed Ca²⁺ as the main leached cation. Concentration increases with time and temp.
Chart: time [min]
| 1 | 3 | 5 | 15 | 30 | 60 | 240
800 | 290.3602 | 4940.0199 | 7071.393 | 8251.7908 | 9318.6348 | 8693.3467 | 10798.4
700 | 808.1714 | 1927.8942 | 4178.3392 | 6964.4045 | 7875.2495 | 8350 | 7035
600 | 448.8844 | 766.4512 | 882.6793 | 1756.4358 | 3218.1019 | 3218.1019 | 5658
500 | 98.4886 | 129.1853 | 274.2016 | 543.7635 | 1151.5755 | 1187.386 | 3493
400 | 130.7629 | 137.5622 | 120.8417 | 171.6617 | 309.8919 | 282.851 | 787
300 | 104.8521 | 102.4297 | 90.2812 | 133.1341 | 117.6568 | 115.7107 | 262.747
200 | 60.7726 | 84.0803 | 73.5196 | 66.0518 | 47 | 67.8982 | 80.5903 | 140
Calcium concentration, Ca²⁺ [mg.kg-1]
SEM
Confirmed Ca-bearing minerals on sample surfaces after experiments.
Pristine sample
Treated Sample
10
Ca²⁺ diffusion linked to Fe²⁺ oxidation?
Fe²⁺ oxidizes
The Fe³⁺/ΣFe ratio increases with increasing temperatures.
T(°C)
Microprobe analysis of polished thick sections of the samples, showed consistent depletion beneath the particle surface.
Calcium depletion, i.e., outward diffusion, seems to be related to the increase of the bulk Fe³⁺⁄ ƩFe ratio.
Ca²⁺+2Fe²⁺=2h•+ 2Fe³⁺
Ca²⁺
CaSO₄
CaSO₄
CaSO₄
Depletion depth
Ca²⁺
Ca²⁺
¹Ludwig-Maximilians-Universität, Munich, Germany, ²Durham University, Durham, U.K., ³Catholic University of Louvain, Belgium.
We noticed that T>500°C and grain sizes <90μm, are conditions that greatly favor SO₂ uptake by glass.
This relation was further tested by preparing haplogranitic glasses with different CaO and FeO wt%; 1-2% and 0-2.5% respectively and conducting high temperature glass-SO₂ experiments. Here we present the results and implications of the experiments.
Chart: Fe³⁺⁄ ƩFe
| 2.3698639298282219E-2
Glass Chip0 | 298.15
Powdered Glass | 298.15
1 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15
3 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15
5 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15
15 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15 | 1173.15
30 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15 | 1173.15
60 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 923.15 | 973.15 | 1073.15 | 1173.15
Glass Chip0 | 298.15
Powdered Glass | 298.15
1 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 973.15 | 1073.15
3 min | 473.15 | 573.15 | 673.15 | 773.15 | 873.15 | 973.15 | 1073.15
Chart: Fe³⁺⁄ ƩFe
| 0.21036585365853658 | 0.28963414634146339 | 0.25304878048780483 | 0.28048780487804881 | 0.24845312138579762 | 0.34805571975635452 | 0.41158536585365851 | 0.21036585365853658 | 0.27743902439024387 | 0.22865853658536589 | 0.20731707317073167 | 0.27560975609756094 | 0.27134146341463405 | 0.27439024390243905 | 0.25609756097560971 | 0.23475609756097565 | 0.23780487804878048 | 0.21951219512195116 | 0.28658536585365857 | 0.26829268292682928 | 0.23170731707317069
1 min | 60.7726 | 104.8521 | 130.7629 | 98.4886 | 448.8844 | 808.1714 | 290.3602 | 309.1197 | 67.6485 | 125.6667 | 144.942 | 307.4627 | 491.0135 | 1096.3166 | 128.1987 | 85.1575 | 65.7171 | 90.8412 | 143.9394 | 188.9443 | 400.2166
3 min | 84.0803 | 102.4297 | 137.5622 | 129.1853 | 766.4512 | 1927.8942 | 4940.0199 | 106.1211 | 136.8929 | 198.3101 | 119.357 | 620.1127 | 1157.4351 | 1572.9685 | 96.5701 | 87.728 | 64.294 | 82.05 | 162.8486 | 300.3654 | 796.0199
5 min | 73.5196 | 90.2812 | 120.8417 | 274.2016 | 882.6793 | 4178.3392 | 7071.393 | 97.6238 | 60.289 | 109.7784 | 237.0869 | 866.2675 | 2526.7664 | 3690.7971 | 84.9934 | 64.4167 | 92.8144 | 98.7531 | 230.9869 | 322.2112 | 524.8793
15 min | 66.0518 | 133.1341 | 171.6617 | 543.7635 | 1756.4358 | 6964.4045 | 8251.7908 | 67.2164 | 82.7529 | 131.0414 | 471.1842 | 1734.1488 | 4031.8371 | 5975.7998 | 80.1266 | 64.3523 | 80.5861 | 173.5489 | 338.7392 | 727.3257 | 1150.6713
30 min | 47 | 117.6568 | 309.8919 | 1151.5755 | 3035.8744 | 7875.2495 | 9318.6348 | 82.3774 | 101.5936 | 191.1765 | 770.6468 | 2112.1333 | 4684.4555 | 7258.6235 | 81.5833 | 85.1981 | 82.5468 | 169.1431 | 382.9187 | 800.8313 | 1873.466
60 min | 67.8982 | 115.7107 | 282.851 | 1187.386 | 3218.1019 | 7034.5315 | 8693.3467 | 94.1558 | 95.3805 | 233.4663 | 899.7838 | 2642.1471 | 5862.3838 | 9487.7927 | 76.4236 | 109.0803 | 82.3774 | 199.0533 | 479.4259 | 1145.0141 | 2220.5614
240 min | 80.5903 | 331 | 787 | 3493 | 5658 | 8350 | 10798.4
Original Glass | 1
Chart: Normalised transect distance
| 0 | 0.11109232330064255 | 0.22218464660128509 | 0.33327696990192762 | 0.44436929320257018 | 0.55546161650321269 | 0.66655393980385524 | 0.7776462631044978 | 0.88873858640514036 | 1
Orig. Sample | 1.66 | 1.66 | 1.66 | 1.66 | 1.66 | 1.66 | 1.66 | 1.66 | 1.66 | 1.66
CaSO₄
CaSO₄
Depletion depth
Ca²⁺
Ca²⁺
CaSO₄
HPG8 vs Natural Rhyolite
Chart: T= 600 1%CaO
| 0 | 0.1 | 1 | 1.5 | 2 | 2.5
5 min | 19.6262 | 58.5578 | 103.1539 | 77.4306 | 219.9703 | 204.9172
15 min | 244.858 | 220.8437 | 331.6352 | 340.6389 | 355.6098 | 712.432
30 min | 458.1745 | 364.4384 | 518.8053 | 535.8911 | 584.0697 | 1112.5622
5 min IG | 866.2675
15 min IG | 1734.1488
30 min IG | 2112.1333
Chart: T= 600 2% CaO
| 0 | 0.1 | 1 | 1.5 | 2 | 2.5
5 min | 293.0977 | 430.9033 | 250.4913 | 359.263 | 261.0553 | 448.506
15 min | 521.2789 | 977.5271 | 527.5324 | 879.235 | 966.5716 | 1296.4613
30 min | 1197.4575 | 1086.9228 | 1298.6906 | 1638.7604 | 1811.6832 | 2355.2662
5 min IG | 866.2675
15 min IG | 1734.1488
30 min IG | 2112.1333
Chart: T= 800 1%CaO
| 0 | 0.1 | 1 | 1.5 | 2 | 2.5
5 min | 387.1745 | 729.2072 | 945.2854 | 831.1862 | 841.4605 | 1708.8959
15 min | 1934.9754 | 1757.5647 | 2123.73 | 2616.8336 | 2329.1707 | 3484.8485
30 min | 2587.4042 | 1955.5994 | 2280.6912 | 3036.2354 | 3606.6763 | 4357.3171
5 min IG | 3690.7971
15 min IG | 5975.7998
30 min IG | 7258.6235
Chart: T= 800 2%CaO
| 0 | 0.1 | 1 | 1.5 | 2 | 2.5
5 min | 664.5053 | 1076.9791 | 1295.4545 | 1290.116 | 1563.789 | 1973.5772
15 min | 2714.8058 | 1822.5452 | 2774.5384 | 2925.917 | 2869.5122 | 4944.7912
30 min | 3510.6126 | 3921.5451 | 4357.1082 | 4297.3373 | 5716.963 | 7178.7641
5 min IG | 3690.7971
15 min IG | 5975.7998
30 min IG | 7258.6235
Oxide wt% | HPG8 (Referred as „H“ in the Grafic) | Natural Rhyolite (Referred as „N“ in the Graph)
SiO2 | 78.28 | 75.95
Al2O3 | 11.76 | 11.91
Na2O | 4.58 | 3.74
K2O | 4.07 | 2.65
CaO | 1 ,2 | 1.7
FeOtotal | 0, 0.1, 0.5, 1, 1.5, 2 ,2.5 | 3.28
SO₂ uptake was tested for a syntetic glass (HPG8⁴) with various FeOt and CaO wt % contents and compared with the experiments¹ carried out with natural rhyolitic glass (calc-alkaline rhyolite from Krafla volcano, Iceland).
Leachate data confirmed that both the addition of CaO and FeOtotal, systematically increased the amount of leached Ca²⁺, thus the growth of CaSO₄, and thereby SO₂ uptake.
4) Holtz et al., 1992 Chem Geol
SO₂ uptake has mostly been regarded as a low-temperature process, where SO₂ is condensed as H₂SO₄ on the ash. However, our work demostrates that high-temperature (>500°C) glass reacts with SO₂; initially chemisorbing it and further reacting to grow surficial CaSO₄.
Moreover, the effect of Fe in this process has never before been studied, and seems to exert a powerful control on Ca²⁺ diffusion (thus SO₂ uptake).
An important implication is that, there is a compositional dependence on Calcium diffusion, that should be taken in consideration when assessing high temperature SO₂ uptake.
5) Suzuki et al., 2005 J Geoph Res
This image is an example of a volcanic plume simulation, where the size particle distribution of ash is been tracked in 3 spatial coordinates, for an eruption of the magnitude of Pinatubo, 1991. Courtesy of Yujiro J. Suzuki.
HPG8 glasses with 2, and 1wt%CaO, upper and lower sets respectively,
And from left to right the FeO total is 0, 0.1, 0.5, 1, 1.5, 2, 2.5 wt%
H
H
H
N
N
N