## Slide 1: Combining Experiments and Modelling to Understand the Role of Potential Sputtering by Solar Wind Ions
Paul Stefan Szabo
Institute of Applied Physics, TU Wien, Vienna, Austria
EGU 2020, May 8th, 2020
Highlights:
Sputtering yields under He2+ irradiation are found to be significantly higher than for He+.
This can be modeled by assuming an additional potential sputtering of O atoms.
For a realistic solar wind scenario, a significant O depletion at the surface and sputtering yield increases of about 40% can be expected.

## Slide 2: Motivation
1
Solar wind sputtering is an important factor in space weathering and exosphere formation on Moon and Mercury [1,2].
We want to investigate effects that are not described by established simulations (e.g. SRIM).
We focus on potential sputtering by multiply charged solar wind ions [3].
© NASA
[1] B. Hapke, J. Geophys. Res.: Planets, 106 (2001), 10039
[3] F. Aumayr, HP. Winter, Philos. Trans. R. Soc. A, 362 (2004), 77
[2] P. Wurz, et al., Icarus, 191 (2007), 486

## Slide 3: Experimental Methods
 Mass changes due to ion irradiation cause changes of the quartz‘s resonance frequeny [1,2]. This enables precise real-time sputtering measurements in ultrahigh vacuum.
Wollastonite (CaSiO3) is used as an analog for pyroxenes on Moon and Mercury.
Thin films were deposited on a Quartz Crystal Microbalance (QCM) with Pulsed Laser Deposition (PLD).
[1] G. Sauerbrey, Zeitschrift für Physik, 155 (1959), 206
[2] G. Hayderer, et al., Rev. Sci. Instrum., 70 (1999), 3696

## Slide 4: Kinetic Sputtering by Singly Charged Ions
Figure: Example of He+ at solar wind energy [1], experimental values for CaSiO3 are compared to simulations with the programs SRIM [2] and SDTrimSP [3].
SDTrimSP with adapted surface binding energies (dashed lines) consistently describes experiments well.
SRIM overestimates measured sputtering yields.
© AAS, The Astrophysical Journal
[1] P.S. Szabo, et al., Astrophys. J, 891 (2020), 100
[2] J.F. Ziegler, M.D. Ziegler, J.P. Biersack, Nucl. Instrum. Methods Phys. Res. B, 268 (2010), 1818
[3] A. Mutzke, et al., IPP-Report, (2019)

## Slide 5: Potential Sputtering by He2+
Figure: He2+ sputtering yields of CaSiO3 were measured under continuous irradiation [1].
The sputtering yield decreases exponentially.
Initial sputtering yields are much higher than the He+ yield (dotted white line).
A steady state is reached after sputtering a few monolayers. Steady state sputtering yields are still higher than for He+.
 Test measurements with Arq+ (q = 2-8) show that the increase of the initial sputtering yield is proportional to the ion‘s potential energy [1].
[1] P.S. Szabo, et al., Astrophys. J, 891 (2020), 100
© AAS, The Astrophysical Journal

## Slide 6: Potential Sputtering: Calculation
Previous measurements with oxides showed that only O atoms are desorbed by potential sputtering [1]. We want to test if O sputtering and subsequent O depletion of the surface is sufficient to describe our measurements. We use a model that has been similarly applied before (e.g. [2]).
Ci ... Surface concentration of element i
ϕ ... Fluence
nA ... Number of atoms in a monolayer
Yi ... Sputtering yield of element i
Cib ... Bulk concentration of element i
 Coupled differential equations (one for each target element, example for O) to describe the change of the surface composition due to sputtering [3]:
Surface concentration
Fluence
Monolayer density
Sputtering yield
Bulk concentration
Surface concentration decrease by sputtering
Surface concentration increase from bulk atoms reaching the surface
 Kinetic sputtering yields are taken from SDTrimSP simulations, an additional potential sputtering term is included for the sputtering yield of O:
γ … scaling factor
Epot ... Ion potential energy
EB ... Band gap of the target material
Scaling factor is taken from measurements
© AAS, The Astrophysical Journal
© AAS, The Astrophysical Journal
[1] M. Sporn, et al., Phys. Rev. Lett., 79 (1997), 945
[2] A.F. Barghouty, et al., Nucl. Instrum. Methods Phys. Res. B, 269 (2011), 1310
[3] P.S. Szabo, et al., Astrophys. J, 891 (2020), 100

## Slide 7: Comparison between Experiment and Model
 The model is used to calculate the steady state sputtering yields from measured initial yields at the start of the irradiation [1,2].
 All measured steady state yields are predicted very well. Therefore, potential sputtering of CaSiO3 can also be described by a preferential sputtering of O atoms.
© AAS, The Astrophysical Journal
© AAS, The Astrophysical Journal
[1] P.S. Szabo, et al., Astrophys. J, 891 (2020), 100
[2] P.S. Szabo, et al., Icarus, 314 (2018), 98

## Slide 8: Consequences for Solar Wind Sputtering
© AAS, The Astrophysical Journal
© AAS, The Astrophysical Journal
 The total solar wind sputtering is calculated for a solar wind composition of 96% H+ and 4% He2+. Results where only kinetic sputtering is taken into account (dashed lines) are compared to calcultions with included potential sputtering (full lines) [1].
A steady state is reached after several 100 years.
Significant O depletion at the surface can be expected.
In the steady state, all sputtering yields are increased by 43%.
[1] P.S. Szabo, et al., Astrophys. J, 891 (2020), 100

## Slide 9: Summary
Sputtering yields for He+ and He2+ were measured at 1 keV/amu. A significant increase by potential sputtering was found for He2+, as well as an exponential decrease with fluence.
The measured steady state sputtering yields could very be well reproduced with a model assuming potential sputtering of O atoms and subsequent O depletion.
Calculations for solar wind sputtering then show that just 4% He2+ will already reduce the O content of the surface significantly. Sputtering yields in the steady state are predicted to be about 40% higher than without potential sputtering.
Further Information and Outlook:
  Significant implantation of He has been observed in our experiments (see H. Biber‘s display EGU2020-9895 in the same session PS1.4/ST4.7).
  Experiments with more realistic mineral samples are planned (see N. Jäggi‘s display EGU2020-3303 in session PS4.4/GD11.2/GI6.10/ST1.11).

## Slide 10: Acknowledgements
H. Biber, M. Brenner, D. Weichselbaum, M. Wappl, A. Niggas, R. Stadlmayr, A. Nenning, M. Sauer, J. Fleig, A. Foelske-Schmitz, F. Aumayr
N. Jäggi, A. Galli, P. Wurz, K. Mezger
M.V. Moro, D. Primetzhofer
A. Mutzke
H. Lammer
M.V. Moro, D. Primetzhofer
Financial support has been provided by the Austrian Science
Fund FWF (Project No. I 4101-N36) and by KKKÖ (Commission
for the Coordination of Fusion research in Austria at the Austrian
Academy of Sciences—ÖAW) as well as the Swiss National
Science Foundation Fund (200021L_182771/1). Support by
VR-RFI (contracts #821-2012-5144, #2017-00646_9 & 2018-
04834) and the Swedish Foundation for Strategic Research (SSF,
contract RIF14-0053) supporting operation of the accelerator at
Uppsala University is gratefully acknowledged.
The computational results presented have been achieved
using the Vienna Scientific Cluster (VSC).