## Slide 1
Biodegradability of single-use polypropylene-based face masks, littered during the COVID-19 pandemic
– a first approach
Heike Knicker and Marta Velasco-Morena
COVID 19
129 billion masks / month (worldwide)
Additional plastic deposal:
5.2 * 104 / month
disposal
of 1%
Threats:
Human health
Animals (unintentional feeding)
nano/microplastics in soil
Transport to rivers/ oceans
What happens to masks after their disposal to soil?
Solid-state NMR Service Unit, IRNAS-CSIC, Sevilla, Spain (e-mail: knicker@irnase.csic.es)
Reasoning
Outer (blue)
Center (filter)
Inner layer
Chart: 
Chart: 
Degradation time
CO2-C production (mg)
Mask
Soil
Mask + soil
C
C
H
H
H
CH3
C
C
H
H
H
CH3
C
C
H
H
H
CH3
21.5 ppm
26.1 ppm
43.8 ppm
Isotactic polypropylene
Statistical Analysis: ANOVA
6 months
Differences indicating degradation?
Solid-state 13C NMR
Respirometry
Total mask
soil+mask cuts (75 % WHC)
Approach
50
0
100
Center
Outer
Inner
ppm
200
100
0
Fresh mask
Degraded mask
Carbonyl C
A: Pool size; MRT: Mean Residence Time
 | Afast | MRTfast | Aslow | MRTslow | R2
 | % | years | % | years | 
soil | 5.2 | 0.114 | 97.1 | 6 | 0.999
outer | 4.6 | 0.008 | 94.9 | 18 | 0.947
center | 3.8 | 0.008 | 95.7 | 7 | 0.981
inner | 4.7 | 0.008 | 94.7 | 31 | 0.780
complete | 4.3 | 0.022 | 96.3 | 21 | 0.946
Very fast pool: 4-5%
MRTslow: 7 to 31 years
“Free” center mask has MRTslow = 7 yrs
Results
All layers have the same chem. composition
No indication for oxidation
Chart: loss of Cmask (% )
| outer | center | inner | outer | center | inner | outer | center | inner | 50-40 ppm | 30-24 ppm | 24-15 ppm
St1 | -2.4483 | -3.1145 | -2.4298 | -2.3983 | -2.8447 | -2.8042 | -0.22483 | 0.95583 | 0.44133
St6 | -3.5612 | -6.8657 | -3.8908 | -1.8946 | -4.2863 | -2.3007 | -0.584 | 0.1516 | 0.18507
Ct1 | -2.1021 | -1.7407 | -1.834 | -1.9614 | -1.6069 | -1.9349 | 1.03 | 0.3475 | 0.76883
Ct6 | -3.8839 | -3.0331 | -3.6401 | -1.9917 | -1.8248 | -2.0281 | -0.16413 | -1.1455 | -0.33507
C-loss per C-group for single (S) / complete (C) masks after 1 / 6 months (t1, t6) of degradation
Center mask is the most chemically affected but:
it is protected if it stays in the “complete” mask
C
C
H
H
H
CH3
C
C
H
H
H
CH3
C
C
H
H
H
CH3
21.5 ppm
26.1 ppm
43.8 ppm
C
C
H
H
H
CH3
C
C
H
H
H
CH3
C
C
H
H
H
CH3
H
H
+
CO2
Cut of “complete” propylene unit