## Slide 1
Mars Red
The magnetic properties of natural pigments: preliminary analyses for their identification in Fine Arts: "the red pigments dilemma"
Chiara Anselmi1, Antonio Sgamellotti2, 3, Manuela Vagnini4, Aldo Winkler5
1 CNR-IRET, Research Institute on Terrestrial Ecosystems, Porano (TR), Italia; 2 Università degli Studi di Perugia, Italia; 3 Accademia Nazionale dei Lincei, Roma, Italia; 4 Laboratorio di Diagnostica per i Beni Culturali, Spoleto (PG), Italia; 5 Istituto Nazionale di Geofisica e Vulcanologia, Roma, Italia
Pigments have discriminable magnetic properties.
Open questions: Role of the grain size, oxidised magnetite (magnetite core with maghemite outer shell), Fe-Al substitution; differences between powders and draftings, commercial and hystorical pigments (green earth).
See the full presentation for yellow, green and blue pigments
0
100
200
300
400
500
600
700
800
T
(°C)
0
200
400
600
800
1000
1200
K (e-6)
600
700
0
600
700
T
[°C]
T
[°C]
0
1/Kt
1/Kt
Red Ochre
0
100
200
300
400
500
600
700
800
T (°C)
0
100
200
300
400
500
600
700
K (e-6)
Caput Mortuum
0
100
200
300
400
500
600
700
800
T (°C)
0
200
400
600
800
1000
1200
1400
1600
1800
K (e-6)
«Hematite»
Chart: 
Red Earth
Chart: 
Ferrimagnetic properties. Accurate Néel (Curie?) temperature. It could be maghemite, but the cooling and heating curves are similar (except for the «bump»).
Antiferromagnetism; hematite+goethite.
Hematite + maghemite, weak antiferromagnetism (high saturation), cooling below heating (maghemite to hematite)
Hematite + new magnetite on heating. Morin transition
Wide susceptibility decrease spectrum: hematite nanoparticles? Cooling curve well below the heating: maghemite inversion to hematite. Morin's transition is barely visible. Weakly antiferromagnetic hysteresis properties.
Notes: The red pigments dilemma: This work is included in the framework of a series of activities about the rock magnetism methods applied to Fine Arts and cultural Heritage. I started measuring the magnetic properties of recent commercial pigments for fine arts, to compare them with similar colours from the eighteenth and nineteenth centuries. Some experiments on archeological pigments were made too. All the pigments showed distinctive and peculiar magnetic properties, controversial and difficult to be understood, especially in the case of red pigments, consisting in a complex mix of oxidised magnetite, hematite and maghemite at various grainsizes. Also green, blue and yellow pigments were interestingly characterized for their magnetic properties.
The idea is to go on with tests on different brands of recent pigments and sources for the ancient ones, with a multidisciplinary approach where the magnetic properties can be complementary to XRF and chemical analyses for their discrimination, restoration and identification in fine arts. This study is coupled to another research about the influence of particulate matter on hystorical buildings, as deduced with magnetic biomonitoring methods.

## Slide 2
Mass magnetic susceptibility
AGM hysteresis properties
Low and high temperature variations of magnetic susceptibility
The magnetic properties of natural pigments: preliminary analyses for their identification in Fine Arts: "the red pigments dilemma"
Chiara Anselmi1, Antonio Sgamellotti2, 3, Manuela Vagnini4, Aldo Winkler5
1 CNR-IRET, Research Institute on Terrestrial Ecosystems, Porano (TR), Italia; 2 Università degli Studi di Perugia, Italia; 3 Accademia Nazionale dei Lincei, Roma, Italia; 4 Laboratorio di Diagnostica per i Beni Culturali, Spoleto (PG), Italia; 5 Istituto Nazionale di Geofisica e Vulcanologia, Roma, Italia

## Slide 3
Chart: Modern Pigments (m3/kg)
| 1_VIVIANITE | 2_BLU_MAYA | 3_TALCO | 4_BLU_PRUSSIA | 5_EMATITE | 6_TERRA_VERDE | 7_COLLA_CONIGLIO | 8_OCRA_ROSSA | 9_OCRA_GIALLA | 10_CAPUT_MORTUM | 11_VINAVIL | P_07_ROSSO | P_08 | P_09
 | 7.9293e-07 | 5.3951e-08 | 4.2273e-08 | 5.4179e-07 | 0.00013486 | 5.0733e-06 | -1.0172e-09 | 9.1695e-05 | 6.5468e-08 | 5.3149e-05 | -1.4899e-08 | 2.969e-06 | 8.4755e-06 | 1.4222e-06
Chart: Low susceptibility samples (m3/kg)
| 1_VIVIANITE | 2_BLU_MAYA | 3_TALCO | 4_BLU_PRUSSIA | 6_TERRA_VERDE | 9_OCRA_GIALLA
 | 7.9293e-07 | 5.3951e-08 | 4.2273e-08 | 5.4179e-07 | 5.0733e-06 | 6.5468e-08
Chart: Thermae Traianae (m3/kg)
| P_07_ROSSO | P_08 | P_09
 | 2.969e-06 | 8.4755e-06 | 1.4222e-06
Chart: Ancient Pigments (m3/kg)
| TERRA_ROSSA_4 | TERRA_GIALLA_3 | TERRA_ROSSA_1 | TERRA_VERDE_5 | TERRA_ROSSA_2
 | 1.1318e-05 | 2.2622e-07 | 1.4734e-06 | 9.3177e-07 | 1.6534e-05
Magnetic susceptibility of the pigments

## Slide 4: The red pigments dilemma: Hematite, Red Ochre , Red Earth , Mars Red, Caput Mortuum

## Slide 5
5 – «Hematite»
a-Fe2O3; antiferromagnetic, susceptibility 0.10-7.60 · 10−6 m3/kg
0
100
200
300
400
500
600
700
800
T
[°C]
0
200
400
600
800
1000
1200
1400
1600
1800
Kt
[E-6]
600
700
T
[°C]
0
1/Kt
600
700
T
[°C]
0
1/Kt
-200
-180
-160
-140
-120
-100
-80
-60
-40
-20
0
20
T
[°C]
394
396
398
400
402
404
406
408
410
412
Kt
[E-6]
Sample: 135 ·10−6 m3/kg
Too much high for hematite...

## Slide 6
«Hematite» drafting
Mostly ferrimagnetic behaviour, probably ascribable to maghemite. The Neél temperature is very precise, probably due to maghemite inversion during heating. The cooling curve is comparable to the heating, this is strange... The bump in the heating curve is typical for maghemite. Very weak unsuturated feateres are present in the drafting; different pigments or steadiness of the sample?

## Slide 7
«Hematite» FORC
Ferrimagnetic PSD FORC features, grainsize 1 to 20 mm for maghemite

## Slide 8
Magnetic Properties and Paleomagnetism of Zebra Rock, Western Australia: Chemical Remanence Acquisition in Hematite Pigment and Ediacaran Geomagnetic Field Behavior
Abrajevitch et al., 2018 https://doi.org/10.1002/2017GC007091
Haematite pigmentation events and palaeomagnetic recording: implications from the Pilbara Print Stone, Western Australia
Abrajevitch et al., 2014, https://doi.org/10.1093/gji/ggu293
Pigmentary Hematite: examples in literature

## Slide 9
8 – Red Ochre Fe2O3 (ferric oxide); maghemite susceptibility (400-600 ·10−6 m3/kg)
0
100
200
300
400
500
600
700
800
T
[°C]
0
200
400
600
800
1000
1200
Kt
[E-6]
600
700
0
600
700
T
[°C]
T
[°C]
0
1/Kt
1/Kt
-200
-180
-160
-140
-120
-100
-80
-60
-40
-20
0
20
T
[°C]
70
80
90
100
110
120
130
140
150
Kt
[E-6]
Sample: 91.7·10−6 m3/kg; too low for maghemite, coexistence of maghemite and hematite

## Slide 10
Red Ochre drafting
The unblocking spectrum between 475 and 675 ° C suggests that hematite nanoparticles dominate the sample, without the drastic drop around the Neél temperature that would be expected for well-formed hematite crystals. The cooling curve is well below the heating as typical for maghemite inversion to hematite. The Morin's transition is barely visible as a change of slope. Weak antiferromagnetic hysteresis properties are present.

## Slide 11
Red Earth Fe2O3 (hematite)
Chart: 
Chart: 
Morin transition

## Slide 12
10 – Caput Mortuum; Fe2(SO4)3
Campione: 53.1 ·10−6 m3/kg
Oxidised magnetite/maghemite + hematite
0
100
200
300
400
500
600
700
800
T
[°C]
0
100
200
300
400
500
600
700
Kt
[E-6]

## Slide 13
Maghemite which is intergrown with hematite, mainly inverts to hematite after heating at about 650 °C, well above its Curie temperature of 610 °C. Al-substitution presumably stabilizes the maghemite structure (γ-Fe2-xAlxO3). The transformation degree is shown to be grain-size dependent and thus kinetically related. In thermomagnetic runs, the three smallest grain-size fractions show an additional inflection point at 350°C, a value commonly reported in the literature for inversion of submicron maghemite

## Slide 14
Mars Red Drafting (Rosso Marte Stesura) FeO3 * nH2O + Al2O3
Goethite + hematite?
0
100
200
300
400
500
600
700
800
T
[°C]
-2
-1
0
1
2
Kt
[E-6]

## Slide 15
2 – Blue Maya: Vegetal indigo with clay
Sample: 0.05·10−6 m3/kg
Very weak susceptibility and hysteresis properties
0
100
200
300
400
500
600
700
800
T
[°C]
-2
-1
0
1
2
3
Kt
[E-6]

## Slide 16
1 –Vivianite
Fe3(PO4)2·8(H2O); paramagnetic, susceptibility between 0.8 e 1.7·10−6 m3/kg
Sample: 0.79·10−6 m3/kg
Paramagnetism, susceptibility decrease with temperature until the formation of new iron oxides (magnetite and hematite).
Weak ferrimagnetic hysteresis properties.
0
100
200
300
400
500
600
700
800
T
[°C]
0
2
4
6
8
10
12
Kt
[E-6]

## Slide 17
4 –Prussian Blue Fe4[Fe(CN)6]3
Sample: 0.54·10−6 m3/kg
Weak magnetic susceptibility and very weak hysteresis properties, relevant formation of magnetic minerals during heating, susceptibility increases during cooling at T<520 °C
0
100
200
300
400
500
600
700
800
T
[°C]
-10
0
10
20
30
40
50
60
70
80
90
100
Kt
[E-6]

## Slide 18
6 –Green Earth (commercial): Fe and Mg aluminosilicates; K[(Al,FeIII),(FeII,Mg](AlSi3,Si4)O10(OH)2
Sample: 5.07 ·10−6 m3/kg
Coexistence of low coercivity magnetic minerals (magnetite with iron sulfides or maghemite)
0
100
200
300
400
500
600
700
800
T
[°C]
-10
0
10
20
30
40
50
60
70
Kt
[E-6]

## Slide 19
Chart: 
Green Earth (historical): Fe and Mg aluminosilicates; K[(Al,FeIII),(FeII,Mg](AlSi3,Si4)O10(OH)2
Paramagnetic hyperbola
The two peaks are shifted towards lower temperatures, with respect to modern sample
Sample: 0.93 ·10−6 m3/kg

## Slide 20
9 – Yellow Ochre
Limonite (2Fe2O3·3H2O, susceptibility 0.7·10−6 m3/kg ); iron hydroxides (FeOOH), goethite (αFeOOH)
Sample: 0.07·10−6 m3/kg
0
100
200
300
400
500
600
700
800
T
[°C]
-2
-1
0
1
2
3
Kt
[E-6]

## Slide 21
Yellow Ochre Drafting
Upside down! Higher coercivity (73 mT)

## Slide 22
Draftings (glues)
Talcum glue
Rabbit glue
Vinavil glue

## Slide 23
Thermae Traianae – susceptibility vs temperature
Prevailing titanomagnetite behaviour, the influence of lithics
P07
0
100
200
300
400
500
600
700
800
T
[°C]
-5
0
5
10
15
20
25
30
35
40
Kt
[E-6]
P08
0
100
200
300
400
500
600
700
800
T
[°C]
-20
0
20
40
60
80
100
120
140
Kt
[E-6]

## Slide 24
P07
P08
P09
Thermae Traianae – hysteresis properties

## Slide 25
Pigments have discriminable magnetic properties.
Hematite: Ferrimagnetic properties. Accurate Néel (Curie?) temperature. It seems maghemite, but the cooling and heating curves are similar (except for the «bump»).
Red Ochre: wide susceptibility decrease spectrum: hematite nanoparticles? The cooling curve is well below the heating: maghemite inversion to hematite. Morin's transition is barely or not visible. Weakly antiferromagnetic hysteresis properties.
Caput Mortuum: hematite + maghemite, weak antiferromagnetism (high saturation), cooling below heating (maghemite to hematite)
Red Earth: hematite + new magnetite on heating. Morin transition
Mars Red: Antiferromagnetism; hematite+goethite.
Green Earth: Similar shape of the magnetothermic curves for modern commercial and hystorical pigments, but the temperatures of peaks are shifted
Yellow Ochre: possible presence of goethite, bad data quality, slight differences between powders and draftings, mechanical effects upon powder hysteresis?
Vivianite, Blue Maya and Prussian Blue: low susceptibility and weak hysteresis properties, different proportions of newly formed magnetite during heating (Prussian Blue > Vivianite > Blue Maya)
Glues: Talcum and Rabbit glues are diamagnetic, vinavil has a ferrimagnetic component superimposed to diamagnetism
Thermae Traianae: The pigment is barely visible on lithic fragments. Thermomagnetic curves of titanomagnetite
Open questions: Role of the grain size, oxidised magnetite (magnetite core with maghemite outer shell), Fe-Al substitution stabilizing maghemite; annealing processes; differences between powders and draftings.