## Slide 1
Degradation of PFAS by activated persulfate
Lin Qian a, Sarah Sühnholz a,b, Julian Bosch b, Katrin Mackenzie a, and Anett Georgi a
SSS 7.5
24th May 2022, EGU22
a Helmholtz-Center for Environmental Research - UFZ, Department of Environmental Engineering, Permoserstr. 15, D-04318 Leipzig, Germany
b Intrapore GmbH, Katernberger Str. 107, D-45327 Essen, Germany

## Slide 2
Introduction
Industrial and consumer products
Per- and polyfluoroalkyl substances (PFAS)
Perfluorooctanoic acid (PFOA)
Environment international 106 (2017): 37-47
Esircworldwide.com Greensciencepolicy.org
PFAS were reported to slip through wastewater treatment plants
Environmental Fate and Transport for Per- and Polyfluoroalkyl Substances (IRTC)
Average DC-F = 532 kJ mol-1
Resistant to conventional reduction, oxidation and biological degradation
Activation
Carboxylic group attack by one-electron transfer
Persulfate-based processes
Subsequent decomposition,
radicals and hydrolysis reactions

## Slide 3
Strategy I
Degradation of PFOA by persulfate activation with FeS

## Slide 4
Degradation of PFOA by persulfate activation with FeS
Chart: cfree,PFOA (mg/L)
| 3.3484132266835141E-3 | 0.6322532970814202 | 1.9384559843861056 | 3.6998522095240247
Trubutecc | 187.9838 | 770.1556 | 1103.5 | 2620.7206
pH=3
pH=5
pH=7
Literature
Sarah Sühnholz
FeS can partially adsorb PFOA
FeS is a catalyst
Sühnholz at al., Chem. Eng. J.(2021)

## Slide 5
Degradation of PFOA by persulfate activation with FeS – Field Test
Field information:
Sum PFAS: 1.1 µg L-1 (70 % sulfate radicals degradable compounds)
Contaminated by fire-fighting foam
Soil mainly fine and medium sand
Permeability coefficient was determined with kf = 1.3 *10-4 m s-1 (Flow velocity = 0.5 m d-1)
Aquifer: floor distance of approx. 17 m and thickness of 5 m
pH = 5
Chromatography effects on the displacement of PFASs in groundwater
Chart: Sum PFAS [µg L-1]
| 43598 | 43633 | 43640 | 43647 | 43662 | 43677 | 43725 | 43777 | 43811 | 43860 | 43900 | 43944 | 43985 | 44008 | 44063 | 44091 | 44117 | 44152 | 44174 | 44223 | 44264 | 44309 | 44343 | 44375 | 44405 | 44438 | 44463 | 44489 | 44552
Summe 27 PFT | 1.1009 | 1.101 | 1.3246 | 0.0021 | 0.0841 | 0 | 0.0198 | 0.0208 | 0.0294 | 0.0406 | 0.044 | 0.091 | 0.1018 | 0.1087 | 0.3375 | 0.2751 | 0.4846 | 0.3558 | 0.358 | 0.1654 | 0.3485 | 0.4173 | 0.4582 | 0.4192 | 3.6024 | 15.6278 | 11.81 | 7.7 | 2.0931 | 6.4

Chart: 
| 43598 | 43633 | 43640 | 43647 | 43662 | 43677 | 43725 | 43777 | 43811 | 43860 | 43900 | 43944 | 43985 | 44008 | 44063 | 44091 | 44117 | 44152 | 44174 | 44223 | 44264 | 44309 | 44343 | 44375 | 44405 | 44438 | 44463 | 44489 | 44552 | 44586 | 44627
Summe abbaubarer Stoffe | 0.9418 | 1 | 0.91576 | 0.9994 | 1.0002 | 1 | 1.0016 | 1.0017 | 1.0024 | 1.0033 | 1.0036 | 1.0061 | 1.0043 | 1.0064 | 1.0023 | 1.0117 | 1.0197 | 1.011 | 1.0111 | 1.0078 | 1.0156 | 1.0092 | 1.0169 | 1.0174 | 1.1416 | 1.1214 | 0.67288 | 0.51896
Normalized concentration of degradable vs. non-degradable PFAS

## Slide 6
Strategy II
Degradation of PFOA by heat-activated persulfate with zeolite

## Slide 7
Limitations: low efficiency in natural water matrix
solute | k (M-1s-1)
 | (1.7 – 4.4) x 105
 | 2.7 x 108
 | 4.1 x 106
 | 9.1 x 106
solute | k (M-1s-1)
 | (1.7 – 4.4) x 105
 | 2.7 x 108
 | 4.1 x 106
 | 9.1 x 106
Rate constants for reaction of sulfate radicals with some solutes
Degradation of PFOA by heat-activated persulfate with zeolite
Reaction conditions: 50 g L-1 BEA35, 240 mM PFOA, 100 mM persulfate, pH0=3.0, and T=70 ⁰C
Zeolite can enrich trace PFOA from water and promote the PFOA degradation by heat-activated persulfate
Qian at al., Chem. Eng. J.(2022)
Lin Qian

## Slide 8
Cost estimation
S2O82-
PFOA-contaminated water
Adsorber with on-site regeneration
Zeolite
ΔT
Zeolite fixed-bed costs
Sodium persulfate costs
Heat energy costs
Overall
20-60 € kg-1 for industrial BEA-type zeolites (36,000 - 108,000€)
10% PFOA breakthrough (Cout/Cin = 0.1) estimated after 43,000 m³ treated water (6 months)
25 € for each regeneration step
35 € for each regeneration step
0.08 – 0.25 € m-3 for 10 cycles
Prevailing large-scale PFAS removal technologies with groundwater pump-and-treat units.
Ion exchange | 0.8–1.7 € m-3
Activated carbon | 0.5–0.9 € m-3
Reverse osmosis | 1.7-2.2 € m-3
PFAS groundwater remediation: State of the art technology and comparison of costs - Handbuch Altlastensanierung und Flachenmanagement (HdA).
Case: 10 m³ h-1 of contaminated water with an inflow concentration of 10 µg L-1 PFOA
Costs determined mainly by the investment costs for the zeolite based on its long-term stability
0.02 – 0.05 € m-3 for 50 cycles
Chart: 
| Zeolite | Other costs
Column1 | 720 | 6
Chart: 
| Zeolite | Other costs
Column1 | 720 | 30
For one regeneration step
Zeolite (99%)
Zeolite (96%)
Treatment of PFOA-contaminated water in a realistic application scenario – zeolite fixed-bed adsorber
Periodically regenerated

## Slide 9
LinkedIn
lin.qian@ufz.de
Contact Info:
Email
Prof. Frank-Dieter Kopinke, Dr. Anett Georgi
Colleagues at Department of Environmental Engineering, Helmholtz-Center for Environmental Research – UFZ, Germany
Acknowledgement:
Thank you!