## Slide 1
Controlling dynamic splitting of Brazilian disc specimens using
Adelaide University Snapback Indirect Tensile test (AUSBIT)
Giang D. Nguyen, Rupesh Verma, Murat Karakus

## Slide 2: Brazilian disc testing
Popular: easy to prepare & set up; adopted in ISRM standard…
Very brittle behaviour observed: snap-back & dynamic behaviour
Storage energy at peak exceeds the dissipative capacity of a single centreline crack
Brazilian disc testing
2
Displacement (mm)
Load (kN)
Snap-back (class II)
ISRM Standard

## Slide 3: Brazilian disc testing: brittle & dynamic behaviour
Fracture in a split second – dynamic behaviour
Impossible to be captured and analysed using advanced image based instrumentation
How can we slow down the fracturing process?
3
Digital Image Correlation
150 Frames/second

## Slide 4: Slowing down fracturing process using AUSBIT
AUSBIT uses indirect displacement control based on lateral displacement
Very brittle behaviour with snap-back can be captured successfully
4
Lateral LVDT to provide feedback to load machine
Whole AUSBIT system
(Adelaide University Snap Back Indirect Tensile Test)
Patented in Australia

## Slide 5: AUSBIT vs. conventional tests: much longer duration of fracturing
Fracturing process with snap-back is over a few hours
This facilitates the use of advanced image-based instrumentation techniques
5
Conventional
Hawkesbury Sandstone
AUSBIT

## Slide 6: AUSBIT: proof that it actually works – true snap-back, not unloading
Acoustic Emission (AE) is used to detect inelastic activities
Significant AE activities recorded during snap-back
6

## Slide 7: AUSBIT tests on different brittle materials
AUSBIT can capture snap-back in a range of brittle materials.
Both Class I and Class II responses can be captured.
7
Bluestone
Iranian Granite
Sandstone
Concrete
Rocks
Load-vertical displacement curves
Normalised Load-vertical displacement curves

## Slide 8: AUSBIT tests on different brittle materials
8
Sandstone
(UCS 50-60 MPa)
( 2 MPa )
Iranian Granite
(UCS 110 MPa)
( 5 MPa )
Concrete
(UCS 30 MPa)
( 3 MPa )
Bluestone
(UCS 140 MPa)
( 10 MPa )
Coal
(UCS 17 MPa)
( 0.9 MPa )
Australian Granite
(UCS 180 MPa)
AUSBIT: Applicable to a wide range of brittle materials
3D Printed Cement Paste
(Bedding Orientation )
2018
2018
2018
2019
2020
2021

## Slide 9: AUSBIT: Conclusions
Thank you for your attention!!!
Indirect displacement control must be used to capture snap-back (class-II behaviour). Our AUSBIT seems to be the first to use it for Brazilian disc testing
AUSBIT works well on a range of brittle materials.
It removes or at least minimises dynamic effects, prolongs the fracturing time, and facilitates the use of advanced image-based instrumentation techniques.