## Slide 1: Effect of organic loading rate on biogas production and concentration of heavy metals and valuable elements in continuous anaerobic co-digestion of manure and reed canary grass Nazia Zaffar, Erik Ferchau, Hermann Heilmeier, and Oliver Wiche Technical University of Bergakademie Freiberg, Biosciences, Bio/Ecology, Freiberg, Germany (naziazaffarqau@gmail.com)
Nazia Zaffar
Ph.D Candidate
Technical University Bergakademie, Freiberg, Germany
Zn
Ge
Ni
REEs
Cr

## Slide 2: PURPOSE OF STUDY
Effect of organic loading rate on the biogas production
Concentration of heavy metal (Cu, Zn, Ni ) and valuable elements (Ge, Zn)

## Slide 3
PROCESS CHAIN
Zn
Ge
Cr
REEs
Ni

## Slide 4: Continues reactor, pH and Temperature
Thermostat
Temp, pH
Gas meter
Digestate outlet
2.3 liter (Substrate)
Propeller
Gas composition
Input Substrate
TU Bergakademie Freiberg | Institut für Biosciences | Telefonnummer: 015901978931 | www.tu-freiberg.de | Vortragender: Nazia Zaffar | Veranstaltungstitel | 27.05.2022

## Slide 5: Result 1 Effect of OLR ([kg VS/(m3 d)] on biogas production
Chart: Gas production [m³/d/m³ FV]
| 1 | 2 | 2.5 | 3 | 3.5 | 4
OLR | 1 | 2 | 2.5 | 3 | 3.5 | 4
pH | 7.1806 | 6.9398 | 6.9839 | 7.2065 | 7.4439 | 7.5

## Slide 6: Result 2 Effect of OLR on concentration of heavy metals (Zn, Cr, Ni) and valuable elements (Ge, REEs)
Chart: OLR
| 1 | 2 | 2.5 | 3 | 3.5 | 4
Zn | 1018.1 | 471 | 480.8 | 309.72 | 376.875 | 295.225
Cr | 23.49 | 5.8084 | 2.5465 | 5.7506 | 15.49 | 10.9853
Ni | 102.5575 | 34.242 | 22.155 | 14.454 | 14.4925 | 12.46
Chart: OLR
| 1 | 2 | 2.5 | 3 | 3.5 | 4
Ge | 0.44394 | 0.35076 | 0.38975 | 0.32617 | 0.31402 | 0.28349
REEs | 12.9901 | 4.1099 | 3.4566 | 3.3103 | 4.214 | 3.1947

## Slide 7: Conclusion
OLR fundamentally impacts gas production and mineral element concentrations in digestate
The effects depend initially on element concentrations in biomass and gas production which potentially offers novel perspectives for optimization of biogas process towards a phytomining of valuable elements and use of digestates as secondary raw materials.