## Slide 1: Biopolymer soil stabilization as protection from slope erosion and shallow sliding
1 Dr., Professor at Faculty of Civil Engineering, University “Ss. Cyril and Methodius” of Skopje
jjosifovski@gf.ukim.edu.mk
2 MSc, Research fellow at Faculty of Civil Engineering, University “Ss. Cyril and Methodius” of Skopje
nikolovskaaleksandra189@gmail.com
Josif Josifovski 1 and Aleksandra Nikolovska Atanasovska 2
EGU22-4236

## Slide 2
Process of creation soil erodibility

## Slide 3: Biopolymer solution – Xanthan gum
Concentration 1.0 %
Art.-Nr. 3557.1
CAS: 11138-66-2
EG-Nr: 2343942

## Slide 4
Silty sand soil | 
Moisture [%] | 23.62
Natural Unit weight [kN/m3] | 18. 82
Specific weight [/] | 2.57
Optimal water content [%] | 17.60
Unit dry weight [kN/m3] | 15.20
Laboratory tests on
natural and biopolymer treated soil
Characterization parameters
 | Biopolymer treated soil |  |  | Natural soil
 | Curing period [days] |  |  | 
 | 1 | 14 | 28 | 0
Strength [kN/m3] | 435.29 | 1132.43 | 1601.68 | 257.09
Deformation [%] | 4.00 | 2.59 | 2.92 | 3.52
Moisture [%] | 13.70 | 7.10 | 6.24 | 14.93
Uniaxial compressive strength (UCS)
Strength & deformation parameters

## Slide 5
II. Experimental testing of natural and biopolymer treated soil
Rainfall 10 liters per hour
1 : 1,5 slope
Test period 3 hours
Natural slope
Eroded soil on untreated slope with an area of 1.0m2 was about 1900gr or soil erosion of 9.5%.
180 "
0 "
Treated slope

## Slide 6: Conclusion
The biopolymer solution can:
Improves strengthening parameters of the soil;
Fills the pores in the soil;
Reduces water infiltration into the soil;
Improves interparticle cohesion;
Increases erosion resistance.
before testing
after testing
Treated soil
Non-treated soil
Thank you for your
Attention !