## Slide 1
Vien
m. Tomatis, F. Turci, J.R. Petriglieri, A. Campopiano, A. Cannizzaro, P. Ballirano, M. Fantauzzi, A. Rossi, A. Bloise, M.R. Montereali, E. Nardi, and A. Pacella
MODELLING THE FENTON REACTION OF amphibole ASBESTOS
EGU General Assembly, 2022
Vienna, 25 May 2022

## Slide 2
Particle-derived free radicals may contribute to the onset of oxidative stress in lung cells
acidic environment
oxidant environment
Surface Fe is responsible for free radical generation
Iron ions exposed at the surface
Fe(II)-O
Fe(III)-O
Fe(III)-OOH
oxidation
coordination
Fe reactivity depends on
To verify whether the surface reactivity is altered when fibers come in contact with
Expected modifications:
Dissolution of surface layers
Iron oxidation
Aim of the work
Free radical generation is one of the physico-chemical features involved in asbestos toxicity

## Slide 3
Na2FeIII2(Fe",Mg)3Si8022(0H)2
Ca2Mg5Si8O22(OH)2
27% Fe
4,5% Fe
Surface chemical composition
Surface reactivity in hydroxyl (•OH) radical generation
Crocidolite
Tremolite
Amphibole asbestos
Incubation in simplified Gamble's solution (pH 4.5)
Incubation in H2O2 solution (pH 7.4)
Surface: 20% Fe (II) and 80% Fe(III)
Bulk: 50% Fe (II) and 50% Fe(III)
Sample preparation
Surface: 30% Fe (II) and 70% Fe(III)
Bulk: 85 % Fe (II) and 15% Fe(III)
Sample characterization
Experimental setup
Spin trapping/EPR in cell-free test
X-ray photoelectron spectroscopy (XPS)
Reaction involved in •OH radical generation
(Fenton reaction)

## Slide 4
1. Effect of acidic environment
Chart: % area of components in XPS Fe signal
| Fe(II)-O | Fe(III)-O | Fe-OOH
Pristine | 29 | 10 | 61
T-24h | 13 | 2 | 85
1 Week | 13 | 10 | 77
Surface composition
No significant alteration of surface composition
Tremolite
Fe speciation
Fe(II) decrease; Fe(III)-OOH increase
Fe oxidation is faster than dissolution
Ca2Mg5Si8O22(OH)2
•OH radical generation
No change of reactivity in •OH radical generation
crocidolite
tremolite
pristine
1 day
7 days
Chart: Mn+/Si ratio
| Fe | Mg | Ca
Pristine | 0.055351 | 0.2214 | 0.1476
24h | 0.053435 | 0.11832 | 0.15267
1Week | 0.046429 | 0.10714 | 0.13571
Chart: Mn+/Si ratio
| Fe | Mg
Pristine | 0.21277 | 0.12766
24h | 0.24031 | 0.015504
1Week | 0.28455 | 0.013415
Mg decrease, Fe increase
Crocidolite
Slight increase of Fe(II)
Surface composition
Dissolution is faster than Fe oxidation
Fe speciation
Na2FeIII2(Fe",Mg)3Si8022(0H)2
Chart: % area of component in XPS Fe signal
| Fe(II)-O | Fe(III)-O | Fe-OOH
Pristine | 21 | 19 | 60
24h | 25 | 23 | 53
1 Week | 28.9 | 23 | 48
Pacella et al., 2021

## Slide 5
Surface composition
Increase of surface iron
Chart: % area of component in the Fe 2p3/2 signal
| Fe (II) - O | Fe (III) - O | Fe (III) - OOH | Fe-P
Pristine | 20 | 18 | 62 | 0
1h | 29 | 16 | 45 | 10
2h | 36 | 29 | 18 | 16
1 week | 28 | 35 | 25 | 12
Increase of Fe(II)-O and Fe(III)-O
Fe speciation
Iron dissolved and then precipitated as phosphate
Fast dissolution promotes Fe from bulk to the surface
Chart: Mn+/Si ratio
| Fe | Mg
Pristine | 0.21277 | 0.12766
1h | 0.22326 | 0.093023
2h | 0.25877 | 0.035088
1 Week | 0.32018 | 0.017544
Promotion of Fe (II) from bulk to the surface enhances •OH reactivity
When no Fe(II) is avalaible (e.g in sample oxidized at 650°C) the reactivity does not increase
2a. Effect of oxidant environment: CROCIDOLITE
pristine
•OH radical generation
Which are the iron ions responsible for the reactivity increase?
Oxidized (only Fe(III))
Increase of the reactivity, mainly in the first hours of incubation

## Slide 6
2b. Effect of oxidant environment: TREMOLITE
Pristine tremolite:
Oxidized tremolite:
sample | Fe(II)/Fe(III)
pristine | 0.43
after 24h incubation H2O2 | 0.34
Reduction of activity due to iron oxidation
Decrease of surface Fe(II)
decrease of reactivity after few hours of incubation in H2O2
constant reactivity
pristine
oxidized
Surface iron distribution
•OH radical generation
Fe(II) + H2O2  Fe(III) + OH- + •OH
(Fenton reaction)

## Slide 7
H2O2 induces remarkable changes in surface reactivity
Conclusion
increase of cation release to maintain charge balance at the surface
Fe(II) oxidation
erosion of the surface
reactivity increases by the exposure of fresh ions from the bulk
iron-poor fibers
iron-rich fibers
surface erosion does not expose enough ions to restore the reactivity
Both asbestos maintain a significant ability to generate free radicals
Thank you