## Slide 1: REE potentials and extraction from waste products
Ana T. Lima
In collaboration with G.M. Kirkelund, F. Ntuli, L.M. Ottosen
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 2: What are rare earth elements?
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 3
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Light: La-Sm
Heavy: Eu-Lu (+Y)

## Slide 4: Background on rare earth elements (REE)
REEs are soft, malleable, ductile, and good electrical conductors
  Used in automotive, nuclear, petroleum, electronic, renewable energy technologies
Group of 17 elements
  Light and heavy REE have been listed as critical
  Essential for current industries
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 5: REE geochemical behaviour in short
Mn+ + Ly− ⇔ ML(n−y)+
where M stands for metal ion, L for ligand, n the oxidation number of M and y the oxidation number of L.
Determinants for REE solubility in porous media:
pH
Sulfate content
Al-, Fe- and Mn-oxides
Carbonates
Lima & Ottosen (2021) Recovering Rare Earth Elements from contaminated soils: Critical overview of current remediation technologies, Chemosphere, 265, 129163
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 6: Different screened wastes
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Incineration
Road Infrastructure
Mining
Sediments from Stormwater ponds
Wood ashes
Coal ashes
Sewage sludge ashes
Mining residue
MSW ashes
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 7: Critical REE Concentrations (mg/kg) – HF digestion
Sample | Y | Nd | Eu | Tb | Dy | Er
Urban retention pond | 11,7 | 11,5 | 0,5 | 0,3 | 1,7 | 1,0
Coal ash | 43,5 | 52,7 | 2,3 | 1,5 | 8,6 | 4,9
Wood bottom ash | 7,0 | 8,3 | 0,4 | 0,2 | 1,4 | 0,8
MSW 1 fly ash | 4,2 | 4,1 | 0,2 | 0,1 | 0,4 | 0,2
MSW (ARC) fly ash | 2,8 | 2,3 | 0,2 | 0,07 | 0,3 | 0,2
Wood fly ash | 11,8 | 14,8 | 0,6 | 0,3 | 2,1 | 1,2
SSA Avedøre | 12,1 | 15,8 | 0,6 | 0,4 | 1,9 | 1,1
SSA Germany | 12,2 | 16,0 | 0,4 | 0,2 | 1,2 | 0,7
SSA Lynetten | 16,2 | 19,5 | 0,7 | 0,4 | 2,4 | 1,4
Harbour sediment | 21,2 | 28,6 | 1,1 | 0,6 | 3,4 | 1,9
Fe-Cr South Africa | 12,3 | 11,8 | 0,5 | 0,3 | 1,9 | 1,1
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 8: Critical REE Concentrations (mg/kg) – HF digestion
Sample | Y | Nd | Eu | Tb | Dy | Er
Urban retention pond | 11,7 | 11,5 | 0,5 | 0,3 | 1,7 | 1,0
Coal ash | 43,5 | 52,7 | 2,3 | 1,5 | 8,6 | 4,9
Wood bottom ash | 7,0 | 8,3 | 0,4 | 0,2 | 1,4 | 0,8
MSW 1 fly ash | 4,2 | 4,1 | 0,2 | 0,1 | 0,4 | 0,2
MSW (ARC) fly ash | 2,8 | 2,3 | 0,2 | 0,07 | 0,3 | 0,2
Wood fly ash | 11,8 | 14,8 | 0,6 | 0,3 | 2,1 | 1,2
SSA Avedøre | 12,1 | 15,8 | 0,6 | 0,4 | 1,9 | 1,1
SSA Germany | 12,2 | 16,0 | 0,4 | 0,2 | 1,2 | 0,7
SSA Lynetten | 16,2 | 19,5 | 0,7 | 0,4 | 2,4 | 1,4
Harbour sediment | 21,2 | 28,6 | 1,1 | 0,6 | 3,4 | 1,9
Fe-Cr South Africa | 12,3 | 11,8 | 0,5 | 0,3 | 1,9 | 1,1
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 9: pH desorption curves
Chart: Coal_Fly
| 11.3 | 9.9699999999999989 | 7.22 | 3.5750000000000002 | 3.38 | 2.3200000000000003 | 1.7149999999999999 | 0.63500000000000001 | 0.3 | 0.14500000000000002 | -0.21000000000000002
Sc | 0.25 | 0.25 | 0.25 | 0.25 | 0.25 | 0.25 | 0.33817 | 2.9536 | 3.1208 | 3.1035 | 3.3206
Y | 0.0625 | 0.0625 | 0.0625 | 3.5983 | 5.5743 | 9.211 | 9.6731 | 10.7335 | 11.3006 | 11.3629 | 11.9238
La | 0.0125 | 0.0125 | 0.0125 | 3.0152 | 6.7887 | 12.842 | 13.6142 | 15.7776 | 16.2946 | 15.9749 | 16.5137
Ce | 0.125 | 0.125 | 0.125 | 5.4333 | 13.1417 | 25.228 | 26.3799 | 29.8971 | 30.3955 | 29.8673 | 30.9798
Pr | 0.025 | 0.025 | 0.025 | 0.70617 | 1.5249 | 2.8523 | 2.9656 | 3.3021 | 3.3346 | 3.3201 | 3.4286
Nd | 0.0625 | 0.0625 | 0.0625 | 0.0625 | 5.9265 | 10.8758 | 11.2381 | 12.3661 | 12.4894 | 12.3717 | 12.7658
Sm | 0.0125 | 0.0125 | 0.0125 | 0.59372 | 1.2784 | 2.25 | 2.3307 | 2.5479 | 2.5654 | 2.5452 | 2.6328
Eu | 0.00625 | 0.00625 | 0.00625 | 0.13085 | 0.24463 | 0.42231 | 0.43379 | 0.47567 | 0.47887 | 0.47566 | 0.52668
Gd | 0.0125 | 0.0125 | 0.0125 | 0.66392 | 1.1836 | 1.9871 | 2.0437 | 2.2236 | 2.2235 | 2.189 | 2.2337
Tb | 0.00625 | 0.00625 | 0.00625 | 0.096791 | 0.16529 | 0.27791 | 0.28806 | 0.31012 | 0.3109 | 0.30769 | 0.31684
Dy | 0.0125 | 0.0125 | 0.0125 | 0.55745 | 0.93784 | 1.557 | 1.5949 | 1.7397 | 1.7458 | 1.7195 | 1.7721
Ho | 0.00625 | 0.00625 | 0.00625 | 0.10969 | 0.17741 | 0.28845 | 0.29926 | 0.32243 | 0.32301 | 0.31877 | 0.32959
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)

## Slide 10: Extraction ratios at pH 0-1
 | Sediment_ Stormwater | Coal_Fly | Wood_Bottom | Wood_Fly | MSW_Nuuk | MSW_ARC | SSA_Avedøre | SSA_Germany | SSA_Lynetten | Mine_SA
Sc | 12 | 15.0 | 19 | 49 | 29 | 40 | 86 | 73 | 59 | 16
Y | 100 | 27.4 | 41 | 67 | 88 | 94 | 100 | 100 | 100 | 16
La | 100 | 25.6 | 45 | 76 | 67 | 2 | 49 | 100 | 40 | 18
Ce | 100 | 24.8 | 40 | 67 | 52 | 4 | 26 | 87 | 20 | 17
Pr | 100 | 22.7 | 42 | 70 | 65 | 18 | 27 | 82 | 20 | 16
Nd | 100 | 24.2 | 44 | 74 | 68 | 39 | 31 | 88 | 23 | 15
Sm | 100 | 24.2 | 42 | 72 | 71 | 67 | 47 | 100 | 30 | 15
Eu | 100 | 22.9 | 35 | 60 | 66 | 62 | 40 | 95 | 35 | 19
Gd | 100 | 22.6 | 39 | 71 | 68 | 67 | 79 | 100 | 50 | 15
Tb | 100 | 21.1 | 33 | 63 | 53 | 69 | 64 | 100 | 39 | 13
Dy | 100 | 20.6 | 33 | 63 | 68 | 71 | 76 | 100 | 47 | 14
Ho | 100 | 19.4 | 29 | 57 | 61 | 65 | 80 | 100 | 51 | 12
Er | 100 | 18.1 | 27 | 55 | 61 | 66 | 88 | 100 | 56 | 13
Tm | 100 | 16.7 | 25 | 52 | 62 | 76 | 76 | 100 | 48 | 12
Yb | 100 | 15.7 | 24 | 52 | 62 | 64 | 76 | 100 | 46 | 13
Lu | 100 | 15.9 | 25 | 48 | 50 | 81 | 77 | 100 | 46 | 13

## Slide 11
Incineration
Road Infrastructure
Mining
Sediments from Stormwater ponds
Wood ashes
Coal ashes
Sewage sludge ashes
Mining residue
MSW ashes
Most promising DILUTE sources of Rare Earth Elements
Highest total REE contents
Highest leachable REE contents

## Slide 12: Final considerations
Extraction and recovery efforts should have into account REE complexation in wastes
Stormwater retention pond sediments have the most acid leachable REE at room temperature
Coal fly ashes and stormwater retention pond sediments are the most promising REE dilute sources
See the link for more details: https://www.sciencedirect.com/science/article/pii/S0375674222000589

## Slide 13: Thank you!
Questions?
Welcome atmli@dtu.dk
Marie Sklodowska-Curie grant agreement no. 713683 (COFUNDfellowsDTU)