## Slide 1
China Agricultural University
Professor Jianying Shang
Phd Chaorui Yan
Nalanda University
Professor Prabhakar Sharma
Coupled impact of proteins with different molecular weight and surface charge on nanoparticle mobility
EGU in 2022

## Slide 2
Three proteins with different
molecular weights
1. bovine serum albumin (BSA)
2. ovalbumin (OVA)
3. α-lactalbumin (A-LA)
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 3
Effect of three proteins on TiO2 stability
Time (min)
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 4
Effect of three proteins on TiO2 stability
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 5
Effect of three proteins on TiO2 stability
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 6
XDLVO Theory
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 7
Absorped layer thickness
Particle | Protein type | Concentration(mg L-1) | ZN/NA(mol m-3) | d (nm) | 1/λ (nm) | R2
TiO2 | BSA | 2 | 0.23 | 4.7 | 5.5 | 0.99
 | BSA | 4 | 0.33 | 4.8 | 5.1 | 0.99
 | BSA | 8 | 0.21 | 5.4 | 5.8 | 0.98
 | BSA | 16 | 0.35 | 5.8 | 5.6 | 0.99
 | OVA | 8 | 0.72 | 5.7 | 5.1 | 0.97
 | A-LA | 8 | 0.58 | 7.5 | 5.6 | 0.97
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 8
Adsorbed protein layer thickness
(Ohshima's soft particle theory)
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 9
Mobility of three proteins
Protein OVA show the strongest mobility
due to more negative surface charge of
OVA protein.
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 10
Effect of three proteins on TiO2 mobility
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 11
Relationship between absorped layer thickness
and NPs mobility
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 12
Mechanism
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 13
Thanks!

## Slide 14
Adsorbed protein layer thickness
(Ohshima's soft particle theory)
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.

## Slide 15
Effect of protein BSA with different
concentrations on TiO2 mobility
Protein OVA show the strongest mobility
due to more negative surface charge of
OVA protein.
Notes: The biochar was produced from wheat straw under 600 degree centigrade.
we use ball mill to grind biochar until it reaches an average particle size of around 600 nanometer。
The image on the left shows the SEM analysis of biochar after grind.