## Slide 1
Session HS5.10
Green infrastructure for sustainable urban hazard management
Giulia Mazzarotto, Matteo Camporese and Paolo Salandin
giulia.mazzarotto.1@phd.unipd.it
Financial support from Alto Trevigiano Servizi S.p.a.
ASSESSING PHYSICAL PROCESSES OF PERMEABLE PAVEMENTS WITH A LARGE-SCALE LABORATORY MODEL

## Slide 2
INTRODUCTION: REALITY IN THE LAB
Reproduce physical processes occurring on permeable pavements by a 1:1 model
Study aim
Flexible and tailored solution that allows water quantity and quality management, dual use of space and no additional land take. Common solution for sidewalks, bike lanes, and low traffic pavements (e.g. parking areas) …
WHY PERMEABLE PAVEMENTS?

## Slide 3
INTRODUCTION: REALITY IN THE LAB
FEATURES
Impermeable area for runoff production
Permeable area
Sloped ramp lined with stones
Reproduce physical processes occurring on permeable pavements by a 1:1 model
Study aim
Flexible and tailored solution that allows water quantity and quality management, dual use of space and no additional land take. Common solution for sidewalks, bike lanes, and low traffic pavements (e.g. parking areas) …
WHY PERMEABLE PAVEMENTS?

## Slide 4
INTRODUCTION: REALITY IN THE LAB
Reproduce physical processes occurring on permeable pavements by a 1:1 model
Study aim
Flexible and tailored solution that allows water quantity and quality management, dual use of space and no additional land take. Common solution for sidewalks, bike lanes, and low traffic pavements (e.g. parking areas) …
WHY PERMEABLE PAVEMENTS?
FEATURES
Impermeable area for runoff production
Permeable area
Sloped ramp lined with stones

## Slide 5
INSTRUMENTS & SENSORS
2
TL14 pressure transducers
1
flow meter
2
tipping bucket flow gauge
6
Teros 32 tensiometers
9
FullJet nozzles
Notes: Frequenza acquisizione dati sistema complessivo, marche sensori

## Slide 6
8 cm
5 cm
15 cm
A
A
30 cm
40 cm
FILTER PACKAGE LAYERS
FILTER PACKAGE
Bedding layer
ASTM #8 (2.36-9.5 mm)
Upper sub-base layer
ASTM #57 (4.75-25 mm)
currently PICP
240x120x80 cm3
Section A-A
Lower sub-base layer
AASHTO #3 (25-50 mm)
Native soil
Sand and clay
Drain pipe
DN100

## Slide 7
RAINFALL SIMULATOR
CURRENTLY TESTING …
… to define optimal configuration that gives the highest degree of rainfall’s uniformity
One-loop pipe network with dint= 2.54 cm
Up to 18 nozzles
36 bekers placed every 50 cm on a 6×1.5 m2
300 cm
150 cm
50 cm
PARAMETERS
α: inclination of the nozzle with respect to the vertical direction
H: height of the nozzle with respect to the planar surface
P: pressure
cN: nozzles’ configuration (for different positions)
Notes: Rainfall intensity between 50 and 150 mm/h

## Slide 8
RAINFALL SIMULATOR
CURRENTLY TESTING …
… to define optimal configuration that gives the highest degree of rainfall’s uniformity
One-loop pipe network with dint= 2.54 cm
Up to 18 nozzles
36 bekers placed every 50 cm on a 6×1.5 m2
… WAITING FOR THE MODEL BUILDING
Notes: Rainfall intensity between 50 and 150 mm/h

## Slide 9
Session HS5.10
Green infrastructure for sustainable urban hazard management
Giulia Mazzarotto, Matteo Camporese and Paolo Salandin
giulia.mazzarotto.1@phd.unipd.it
Financial support from Alto Trevigiano Servizi S.p.a.
TO EARLY FOR CONCLUSIONS, BUT…
QUESTIONS/SUGGESTIONS?