## Slide 1: Progressing experimental methods for the hydrological characterization of structural soil substrates
Federal Ministry for Agriculture, Forestry, Regions and Water Management
Sebastian Rath1,2, Anna Zeiser1,2, Monika Kumpan1, Peter Strauß1, Thomas Weninger1
EGU General Assembly 2023
Vienna, 28.04.2023
1
2
Conclusions
Results
Methods
Introduction
Objectives

## Slide 2: Structural soil substrates
Special urban tree substrates
Main functions:
  Extended rooting space for urban trees under sealed surfaces
  Nature-based-solution for urban rainwater management
3:0 Landschaftsarchitektur
Objectives
Conclusions
Results
Methods
Introduction
Zeiser et al., 2021; Grimm et al., 2021

## Slide 3: Structural soil substrates
Substrate components:
  Coarse gravel (ensuring load bearing capacity)
  Fine growing substrate (functioning as rooting space)
3:0 Landschaftsarchitektur
Zeiser et al., 2021; Grimm et al., 2021
Objectives
Conclusions
Results
Methods
Introduction

## Slide 4: Structural soil substrates
  Water capacity
  Hydraulic conductivity
  Air capacity
3:0 Landschaftsarchitektur
Introduction
Objectives
Conclusions
Results
Methods

## Slide 5: Laboratory method
Phase 1:
Saturation & Free Drainage
Phase 2:
Multi-Step-Outflow
Phase 3:
Evaporation
Objectives
Conclusions
Results
Methods
Introduction

## Slide 6
Ecosystem services:
  Cooling through shading and transpiration
  Carbon sequestration
  etc.
To fulfill ecosystem services properly, urban trees must be:
  vital
  able to grow old
Moser-Reischl et al., 2017
Brandenburg et al., 2015
Urban trees
Objectives
Conclusions
Results
Methods
Introduction

## Slide 7: Challenges for urban trees
Low life expectancy in cities
Reasons:
  Urban-Heat-Island-Effect
  Limited rooting space
  Soil sealing
  Soil compaction
  etc.
Brandenburg et al., 2015; Benk et al., 2020
Objectives
Conclusions
Results
Methods
Introduction
Roloff & Kehr, 2013

## Slide 8: Structural soil substrates
USA: Structural soils – since 1990s
Sweden: Stockholm system – since 2009
Austria: Sponge city substrate for urban trees – since 2018
Special urban tree substrates under sealed surfaces (streets, pavements etc.)
Systems for stormwater retention and infiltration
3
Air- or water-filled pores
Fine growing substrate
Coarse gravel
Contact points (load distribution)
Objectives
Conclusions
Results
Methods
Introduction
Bassuk et al., 2015; Embrén et al., 2009; Grimm et al. 2021

## Slide 9: Structural soil substrates
Substrate components:
  Coarse gravel
    ensures load bearing capacity
    stable pore volume
    Granite or dolomite
    Grain size between 3 and 15 cm (in Austria 9 to 15 cm)
  Fine growing substrate
    Rooting space
    Certain storage capacity for water and nutrients
    Flushed into the voids of coarse gravel
    In Austria mostly Sand (0/4 mm) with compost and biochar
3:0 Landschaftsarchitektur
Objectives
Conclusions
Results
Methods
Introduction
Zeiser et al., 2021; Grimm et al., 2021; Murer, 2022

## Slide 10: Structural soil substrates
Main goal: developing a lab method to determine
  retention capacities at different matric potential states
  saturated hydraulic conductivity
  total pore volume
3:0 Landschaftsarchitektur
Introduction
Objectives
Conclusions
Results
Methods

## Slide 11: Laboratory method
Phase 1:
Saturation & Free Drainage
Phase 2:
Multi-Step-Outflow
Phase 3:
Evaporation
  Saturated hydraulic conductivity
  Total pore volume
  Water capacity after 2 hours of free drainage
  Volumetric water content at matric potential states ranging from -60 to -100 hPa
  Volumetric water content at matric potential states ranging from -100 to -700 hPa
Objectives
Conclusions
Results
Methods
Introduction

## Slide 12: Laboratory method
Sample preparation
Conclusions
Objectives
Conclusions
Results
Methods
Introduction

## Slide 13: Laboratory method
Phase 1:
Saturation & Free Drainage
  Saturated hydraulic conductivity
  Total pore volume
  Water capacity after 2 hours of free drainage
Objectives
Conclusions
Results
Methods
Introduction

## Slide 14: Laboratory method
Phase 2:
Multi-Step-Outflow
  Volumetric water content at matric potential states ranging from -60 to -100 hPa
Objectives
Conclusions
Results
Methods
Introduction

## Slide 15: Laboratory method
Phase 3:
Evaporation
  Volumetric water content at matric potential states ranging from -100 to -700 hPa
Objectives
Conclusions
Results
Methods
Introduction

## Slide 16: Connected field monitoring sites
Street tree lysimeters, Vienna
Objectives
Conclusions
Results
Methods
Introduction
Open air laboratory, Graz

## Slide 17: First results
Objectives
Conclusions
Results
Methods
Introduction
growing substrate |  | BD | Ks | TPV | WC2h | AC2h | WC1.8 | AC1.8
 |  | g cm-3 | m d-1 | cm3 cm-3 | cm3 cm-3 | cm3 cm-3 | cm3 cm-3 | cm3 cm-3
 | A | 1,98 | 20,8 | 21,7 | 9,8 | 12,0 |  | 
 | A | 1,98 | 29,3 | 21,0 | 10,2 | 10,8 |  | 
 | A | 1,98 | 33,8 | 23,1 | 10,3 | 12,8 |  | 
 | A | 1,94 | 24,7 | 25,3 | 11,6 | 13,6 | 5,9 | 19,4
 | A | 1,99 | 22,8 | 26,1 | 14,3 | 11,8 | 4,7 | 21,4
 | B | 2,02 | 23,1 | 24,0 | 11,5 | 12,6 |  | 
 | B | 2,04 | 23,8 | 23,2 | 11,6 | 11,7 |  | 
 | B | 2,01 | 42,2 | 25,1 | 9,9 | 15,2 | 6,4 | 18,7
 | B | 2,01 | 39,8 | 25,9 | 9,7 | 16,2 |  | 
 | B | 2,02 | 48,7 | 26,3 | 9,4 | 16,9 | 7,5 | 18,9
mean | A,B | 2,00 | 30,88 | 24,2 | 10,8 | 13,35 | 6,3 | 18,3
mean | A | 1,97 | 26,3 | 23,5 | 11,2 | 12,2 | 5,7 | 17,8
 | B | 2,02 | 35,5 | 24,9 | 10,4 | 14,5 | 6,9 | 18,8
standard deviation | A | 0,019 | 5,23 | 2,21 | 1,84 | 1,07 | 0,57 | 2,62
 | B | 0,011 | 11,51 | 1,29 | 1,03 | 2,29 | 0,76 | 0,14
CV | A | 0,010 | 0,20 | 0,09 | 0,16 | 0,09 | 0,10 | 0,15
 | B | 0,005 | 0,32 | 0,05 | 0,10 | 0,16 | 0,11 | 0,01
significant difference | Yes/No | Y | N | N | N | N | N | N
Hydrological properties of structural soil substrates with growing substrates A (sand, compost, biochar, silt) and B (sand, compost, biochar) flushed into 25% of volume constantly.
Abbreviations:
BD = bulk density,
Ks = saturated hydraulic conductivity,
TPV = total pore volume,
WC2h = water capacity after 2 h drainage,
AC2h = air capacity after 2h draining,
WC1.8 = water capacity at pF = 1.8,
AC1.8 = air capacity at pF = 1.8,
CV = coefficient of variance (CV = standard deviation / mean).
Significant differences between growing substrates were calculated by two-sided Student´s t-test at significance level α = 0.05.

## Slide 18: First results
Chart: Water retention curve (pF curve)
Structural soil substrate - growing substrate B | 24.0412 | 11.4819 | 7.3 | 4.43 | 3.74 | 3.02 | 2.93 | 2.62 | 2.32 | 2.21 | 0.71
Objectives
Conclusions
Results
Methods
Introduction
  Percolating water (pF < 1,8)
  Plant available water (pF = 1,8 to 4,2)
  Bonded water (pF > 4,2)

## Slide 19: First results
Objectives
Conclusions
Results
Methods
Introduction
  Percolating water (pF < 1,8)
  Plant available water (pF = 1,8 to 4,2)
  Bonded water (pF > 4,2)

## Slide 20: Conclusions and Outlook
Introduction
Objectives
Conclusions
Results
Methods
This study represents a first step for developing appropriate methodology for a practicable hydrological characterization of structural substrates for urban tree sites. Several theoretical and methodological questions were solved, multiple others came up in the study and therefore remain open.
Further results from already established monitoring field sites will improve knowledge. In this study, the focus was on testing and progressing methodology which is broadly applicable in engineering practice.
Open question: selection of appropriate model(s) for parametric hydraulic characterization and modeling; e.g. dual-porosity, dual-permeability, gravity-driven module …?

## Slide 21: References
3:0 Landschaftsarchitektur. (n.d.). Das Schwammstadt-Prinzip für Bäume. Retrieved from: https://www.schwammstadt.at/. 10.8.2022.
Bassuk, N., Denig, B. R., Haffner, T., Grabosky, J., Trowbridge, P. (2015). CU-Structural Soil - A Comprehensive Guide. Ed. Denig, B. R. Urban Horticulture Institute, Cornell University. Retrieved from: http://www.hort.cornell.edu/uhi/outreach/pdfs/CU-Structural%20Soil%20-%20A%20Comprehensive%20Guide.pdf. 9.3.2022.
Benk, J., Artmann, S., Kutscheidt, J., Müller-Inkmann, M., Streckenbach, M., Weltecke, K. (2020). Praxishandbuch Wurzelraumansprache. Möhnesee: Arbeitskreis Baum im Boden.
Brandenburg, C., Damyanovic, D., Reinwald, F., Allex, B., Gantner, B., Czachs, C. (2015). Urban Heat Islands. Strategieplan Wien. Vienna: Magistrat der Stadt Wien, Umweltschutzabteilung - MA 22. Retrieved from: https://www.wien.gv.at/umweltschutz/raum/uhi-strategieplan.html. 26.3.2022.
Grabosky, J., Haffner, E. & Bassuk, N. (2009). Plant Available Moisture in Stone-soil Media for Use Under Pavement While Allowing Urban Tree Root Growth. Arboriculture & Urban Forestry, 35 (5): 271–278. doi:10.48044/jauf.2009.041.
Grimm, K., Murer, E., Schmidt, S. (2021). Das Schwammstadtprinzip für Stadtbäume in Österreich. Entstehung, Funktionsweise, Herausforderungen, Umsetzungen. Schwammstadt - Versickerung 2.0? (S. 51–55). Conference paper from Aqua Urbanica 2021, Innsbruck: Österreichischer Wasser- und Abfallwirtschaftsverband (ÖWAV).
Moser-Reischl, A., Rötzer, T., Pauleit, S. (2017). Stadtbäume: Wachstum, Funktionen und Leistungen – Risiken und Forschungsperspektiven. ALLGEMEINE FORST UND JAGDZEITUNG, 188 (5–6): 94–111. doi:10.23765/afjz0002006.
Murer, E. (2022, March 15). Schwammstadt für Stadtbäume. Erfahrungen & Herausforderungen. PowerPoint-Präsentation at Workshop Jägerhausgasse, Vienna.
Roloff, A., Kehr, R. (2013). Bäume in der Stadt: Besonderheiten - Funktion - Nutzen - Arten - Risiken ; 12 Tabellen. Stuttgart (Hohenheim): Ulmer.
Rose, B. (2020). Tree Pits with Structural Soils - Practice Note (Version 1.2). Retrieved from: https://www.researchgate.net/publication/341343983_Tree_Pits_with_Structural_Soils_-_Practice_Note_Version_12. 16.12.2022.
Zeiser, A., Murer, E., Schmidt, S., Kumpan, M., Strauss, P., Weninger, T. (2021). Schwammstadt für Stadtbäume. Funktionsorientierte Substratentwicklung am Beispiel des multifunktionalen Wurzelraums. Schwammstadt - Versickerung 2.0? (S. 92–96). Conference paper from Aqua Urbanica 2021, Innsbruck: Österreichischer Wasser- und Abfallwirtschaftsverband (ÖWAV).
Conclusions
Introduction
Objectives
Results
Methods