## Slide 1
Simulating Radiation and Thermal Cycling Effects in Lunar Construction Materials
Adrija Bhowmick
PhD Student – Institute of Physics
University of Debrecen
Research Assistant
HUN-REN Atomki
Supervisor: Prof. Nigel J. Mason

## Slide 2
Settlement
Notes: As we enter the era where space exploration has stepped onto the Moon (our natural satellite), new plans and missions are developed almost every day, driven by the urge to expand human presence beyond Earth which leads to establishing permanent bases in space premises. Now for constructing any bases, it is crucial to have materials that can endure and perform reliably under the harsh conditions of space and materials science becomes a fundamental aspect of space exploration.

## Slide 3
Lunar Conditions
ISRU-based materials for Lunar Habitat
Regolith
Composition:
Challenges:
Radiation
+
+
+
Temperature
Malla, Ramesh B.; Brown, Kevin M. (2015).
100 K
400 K
Solar Wind Simulator, AQUILA

## Slide 4
Research Framework
1. Experiments: Ion Irradiation and Temperature Cycling
1.3. Results Obtained
Structural analysis.
Scanning Electron Microscopy (SEM).
X-ray Diffraction (XRD).
Energy-Dispersive X-ray Spectroscopy (EDS)
1.1. Samples
HDPE with a density of 0.95 g cm–3.
15 mm in diameter.
2 mm in thickness.
1.2. Experimentation
Irradiation: 2x1016 ions cm–2, 10 keV protons, at 300 K.
Temperature cycling: 200K  350 K.​
Irradiation + temperature cycling.
Experiments were performed by J. Cousins, University of Kent, at HUN-REN ATOMKI, Hungary.

## Slide 5
Research Framework
2. Modelling: Molecular Dynamics (MD) Simulation
2.1. Model Construction
Amorphous PE model made using CHARMM-GUI [5].
Optimised using MBN Explorer [6].
SiO2 optimised using the Tersoff potential [7,8].
2.2. Simulations
Temperature cycling performed between 100 and 400 K.
Repeated over 8 cycles.
2.3. Results Obtained
Structural analysis.
Radial distribution function (RDF) analysis.
100–400 K

## Slide 6
Research Framework
1. Experiments: Ion Irradiation and Temperature Cycling
2. Modelling: Molecular Dynamics (MD) Simulation
3. Validation & Integration
Compare simulation outputs with experimental results.
Refine models and parameters.
Model Refinement
Experimental Feedback

## Slide 7
Preliminary Results & Remarks
1. Experiments: Ion Irradiation and Temperature Cycling
1.1. High Density PE
b) After Irradiation:
c) After Irradiation + Temperature Cycle:
a) After Temperature Cycle:

## Slide 8
Preliminary Results & Remarks
1. Experiments: Ion Irradiation and Temperature Cycling
b) After Irradiation:
a) Before Irradiation:
Energy-Dispersive X-ray Spectroscopy (EDS) Spectrum
1.2. Concrea (Lunar Regolith + Urea)

## Slide 9
Preliminary Results & Remarks
2. Modelling: MD Simulation
b) After Temperature Cycle:
a) Before Temperature Cycle:
2.1. Amorphous PE
Combining irradiation experiments with atomistic modelling provides a pathway toward understanding and predicting material performance under the coupled radiation–thermal environment of the Moon.

## Slide 10: Thank You For Your Attention
Experimental Molecular Physics Research Group
adrija.bhowmick@atomki.hu
Poster: F2.55